## Slide 1: Heavy Ion Beam Analysis of Ion Implanted Polymer Nanocomposites Master of Applied Science (Industrial Physics)
Student: Mashamba Dakalo Rollet
Supervisor: Prof M. Msimanga [TUT-iThemba LABS]
Co-Supervisor: Dr T.P. Sechogela [iThemba LABS]

## Slide 2
Introduction
Problem statement
Aim & objectives
Experimental setup
Results and discussion
Conclusion
References
Acknowledgements
Presentation outline

## Slide 3
Ion Beam Analysis (IBA) is a cluster of nuclear analytical techniques used to determine elemental composition and depth profiles of layers in solid samples.
The analysis is based on interaction between the incoming beam of ions and the target material.
The interaction may lead to emission of particles which characterize the elemental concentration and depth profile of the target material through the detector system.
IBA Techniques | Detection mechanism | Unique strength
RBS (Rutherford Backscattering Spectroscopy) | Detection of backscattered particles | Analysis of heavy elements in light matrices
ERDA (Elastic Recoil Detection Analysis) | Detection of elastically recoiled particles | Analysis of light elements in heavy matrices
1. Introduction

## Slide 4
1.1. ERDA theoretical considerations
Schematic diagram of scattering and recoil events, before and after collision.
Where M1 is the mass of the projectile ion, M2 is the mass of the target element.
ES and Er are energies of scattered and recoiled ions respectively
α is the scattering angle and β is the recoil angle
Energy Er of the recoiled atom:
= Kr = cos2 α
Where Kr is the recoil kinematic factor
Probability σ of a target atom to be recoiled in a particular direction α:
=
σ Z12
Where E0 is given in MeV, e2 = 1.4398 x 10-13 MeV.cm and is in cm2. Z1 and Z2 are atomic numbers of the projectile and target element respectively
Kinematics
Cross section

## Slide 5: 2. Problem statement
During ERD analysis using heavy ions, the projectile beam may cause damage to the sample under analyses, this is especially true the case of soft target materials like polymers.
It then becomes necessary to determine the most suitable experimental conditions, i.e beam type, energy and fluence to minimize sample damage during analysis.
3. Aim
The aim of this study was to optimize the Time of Flight-ERDA set up at iThemba LABS to minimize beam dose on organic polymeric films during analysis, but still obtain sufficient measurement statistics.
Time of flight ERDA setup at iThemba LABS, TAMS

## Slide 6
4. Objectives
Ion implantation of polyethylene terephthalate (PET) with different ion fluences of 5 x 1015 , 2 x 1016 , 5 x 1016 ions/cm2 with 80 keV Ti+ ions.
Carrying out RBS to confirm implantation fluence and thickness of the modified layer.
Carrying out ERDA depth profiling using 18 MeV 63Cu5+ beam.
Carrying out ERDA depth profiling using 30 MeV 197Au7+ beams.

## Slide 7
5. Results and discussions

## Slide 8
5.1. SRIM/TRIM simulations
3D ion distribution of ions as a function of depth in PET

## Slide 9
5.2. RBS: Pristine PET
RBS experiment was performed with 2 MeV He+ ions.
The observed edges correspond to He+ backscattered from PET surface composed of carbon (C), oxygen (O) and hydrogen (H).
It was expected that the hydrogen edge will not appear because He+ does not backscatter from H.
Experimental
Simulated
Experimental and simulated RBS spectra of pristine PET sample

## Slide 10
(a) PET-Ti 5 x 1015 ions/cm2
(b) PET-Ti 2 x 1016 ions/cm2
(c) PET-Ti 5 x 1016 ions/cm2
Thickness of the implanted layer was found to be approximately 1300 x 1015 at./cm2 or 135 nm.
(c)
(a)
(b)
5.2.1 RBS : Implanted PET

## Slide 11
Coincidence measurement of flight time and energy during ERDA experiments lead to generation of a mass separated 2-D scatter plot.
ERDA measurements were done using 18 MeV 63Cu5+ and 30 MeV 197Au7+ beams at constant current of 11 nA.
Potku software, developed by the Finnish group has been recently developed for depth profiling ERD analysed samples.
2D ToF-Energy scatter plot of recoils from analysis of PET with 18 MeV Cu5+ beam
5.3. ERDA: Pristine PET

## Slide 12
5.3.1. Comparative ERD analysis with 30 MeV 197Au7+ and 18 MeV 63Cu5+ beams
Depth profile of 30 MeV Au7+ analysed pristine PET
Depth profile of 18 MeV Cu5+ analysed pristine PET
C
H
O
C
H
O

## Slide 13
5.3.2. Comparative ERD analysis with 30 MeV 197Au7+ and 18 MeV 63Cu5+ beams
Experimental observations
Theoretical considerations
Au recoil-X-section
Cu recoil-X-section
197Au7+ analysis
63Cu5+ analysis
Ф =
197Au7+ time of analysis (t) & fluence (Ф) : 9 min & 9.8 x 1012 ions/cm2
63Cu5+ time of analysis (t) & fluence (Ф) : 20 min & 3 x 1013 ions/cm2
Variation of recoil cross section with target mass for 197Au and 63Cu incident beams
Energy spectra for hydrogen yield in counts for 30 MeV 197Au7+ and 18 MeV 63Cu5+ incident beams

## Slide 14
5.3.3. Depth profiles of ion implanted PET with 30 MeV 197Au7+ beam
C
H
O
Ti
C
H
O
Ti
C
H
O
Ti
5 x 1015 ions/cm2
2 x 1016 ions/cm2
5 x 1016 ions/cm2

## Slide 15
It is preferable to use heavy ions during materials analyses due to obtainable sufficient experimental statistics compared to light ions.
Beam induced damages can be minimized by reducing the time of analysis.
During ion implantation polymers undergo carbonization, dehydrogenation and oxidation.
The occurrence of these processes may result in improved electrical and optical properties of the polymers.
6. Conclusion

## Slide 16
Schmidt B. et. al. Materials Analysis by Ion Beams. Ion Beams in Materials Processing and Analysis, (2012), 301–376. doi:10.1007/978-3-211-99356-9_6
Ziegler J F. SRIM 2013 [Cited 2021/07/08]. Available from www.srim.org.
Arstila K. et.al. Potku-New analysis software for heavy ion elastic recoil detection analysis. Nucl. Instr. Meth. B (2014); 331:34-41. https://doi.org/10.1016/j.nimb.2014.02.016.
Moro M.V. et al. Accurate high-resolution depth profiling of magnetron sputtered transition metal alloy films containing light species: A multi-method approach, Thin Solid Films, (2019), https://doi.org/10.1016/j.tsf.2019.137416
A. Mackova, P. Malinsky, R. Miksova, Characterisation of PEEK , PET and PI implanted with 80 keV Fe+ ions to high fluencies, Nuclear Instrument and Methods in Physics B 331 (2014) 176-181
7. References

## Slide 17
8. Acknowledgements
Tshwane University of Technology
NRF-iThemba LABS
Prof M. Msimanga
Dr T.P. Sechogela

## Slide 18
Thank You
?