## Slide 1: Investigation of a novel iron-based cubic compound RhFe3C
Nyawasedza Magoda
Materials Physics Research Institute, School of Physics
University of the Witwatersrand, Johannesburg, SA
Supervisors:
Prof. Deena Naidoo
Dr. Abhishek Pandey

## Slide 2: Outline
Introduction.
Background on
Motivation for studying
2. Experimental Details + Results.
3. Conclusion.

## Slide 3: Introduction – B
Synthesis of :
Two step process combining high temperature sintering reaction with a low temperature nitriding reaction.
Reference: A. Houben et al. Chem. Mater. 21, 784-788 (2009)
RhFe3N
Fe0.5Rh0.5
1a: Rh
1b: N
3c: Fe
2. Two phases were formed:
- with a = 3.8337
- with a = 2.983

## Slide 4: Introduction – B
Reference: A. Houben et al. Chem. Mater. 21, 784-788 (2009)
Rietveld refinement+ Mössbauer analysis prove that the Rh, N and Fe atom occupies Wyckoff position 1a, 1b and 3c respectively.

## Slide 5: Introduction – B
Reference: A. Houben et al. Angew. Chem. Int. Ed.44. 7212 (2005)
Soft ferromagnetic material.
Applications:
High density storage material.
High performance magnetic recording devices.

## Slide 6: Introduction - RhFe3C
Aim of work:
Synthesize and study a new cubic compound similar to
- No impurities.
- High with better magnetic properties.
Synthesis:
Arc melting.
Experimental techniques:
Powder X-ray Diffraction
Mössbauer Spectroscopy
Heat Capacity
Resistivity
Wavelength Dispersive Spectroscopy

## Slide 7: Experimental Details & Results

## Slide 8: X-Ray Diffraction
A Le Bail fit was performed.
No impurities found.
Cubic crystal structure with lattice parameter a = 5.8907.
A detailed Rietveld analysis is underway.
Detector
Mo X-ray tube
theta-theta goniometer
Bruker D9 diffractometer, Mo radiation with a wavelength of .

## Slide 9: Mössbauer Spectroscopy
Reference: M. Darby Dyar et al. Annu. Rev. Earth Planet. Sci. 34:83–125 (2006)
Recoil effect during radiation emission/absorption.
Energy level diagrams with corresponding spectra observed.
Electric monopole Interaction (Isomer shift).
Electric Quadrupole Interaction (Quadrupole splitting).
Magnetic Dipole Interaction (Magnetic splitting).

## Slide 10: Mössbauer Spectroscopy
Mössbauer drive
Absorber
Detector
Transmission Mössbauer Spectroscopy set-up.
Lead shield
Amplifier
HV Power supply
Drive unit
Lead shield
Amplifier
HV Power supply
Drive unit
Source

## Slide 11: Mössbauer Spectroscopy
Component |  | IS (mm/s) |  | Relative area (%) | Assignments
Sextet 1 | 39.19 | 0.14 | 0.03 | 21.61 | Fe3+
Sextet 2 | 36.18 | 0.09 | 0.01 | 35.59 | Fe3+
Sextet 3 | 33.75 | 0.04 | 0.003 | 41.77 | Fe3+
Singlet | - | 0.01 | - | 1.02 | -
Component |  | IS (mm/s) |  | Relative area (%) | Assignments
Sextet 1 | 39.19 | 0.14 | 0.03 | 21.61 | Fe3+
Sextet 2 | 36.18 | 0.09 | 0.01 | 35.59 | Fe3+
Sextet 3 | 33.75 | 0.04 | 0.003 | 41.77 | Fe3+
Singlet | - | 0.01 | - | 1.02 | -
Chart: Velocity [mm/s]
RhFe3C

## Slide 12: Heat Capacity
Temperature: 2K – 250K
Sommerfeld coefficient.
Fraction of Einstein contribution to the
Electronic cabinet
Dewar
Linear transport motor
237

## Slide 13: Heat Capacity

## Slide 14: Conclusion
RhFe3C is a single-phase compound which has a cubic structure with a = 5.8907 .
Three different iron sites were identified with oxidation state Fe3+ .
One of the iron phases was found to be the same a
Identification of iron phases will be confirmed when detailed analysis of XRD data has been performed.
Analysis of the Heat capacity data resulted in
.

## Slide 15: Future Plans
The following research works will be conducted:
Detailed XRD analysis.
Magnetization measurements.
Magnetoresistance measurements.

## Slide 16: Acknowledgements
Collaborators: Abhishek Pandey1, D. Naidoo1 , S. Chakraborty2, S. Gupta2, S. Dan3, A. Shnier4, D. G. Billing4, Chandan Mazumdar2 and D. Wamwangi1 .
1Materials Physics Research Institute, School of Physics, University of the Witwatersrand, Johannesburg, Gauteng 2050, South Africa.
2Condensed Matter Physics Division, Saha Institute of Nuclear Physics, Kolkata, Bengal 700064, India.
3Department of Physics, University of Burdwan, Burdwan, Bengal 713104, India.
4School of Chemistry, University of the Witwatersrand, Johannesburg, Gauteng 2050, South Africa.
Supported by:

## Slide 17: Any Questions?