## Slide 1: Enigmatic Structure Property Behaviour in SOFC & SOEC materials, and the importance of Synchrotron Techniques
By
Dave Billing
University of the Witwatersrand,
Johannesburg, South Africa

## Slide 2: Global sustainability challenges

## Slide 3: Energy Poverty
https://www.odi.org/coal-and-poverty-faq-energy-access

## Slide 4
Energy
Materials
Solar Cells
Batteries
Fuels cells / SOFC
Property
Structure
Function
Performance
Adam Shnier
Michelle Thiebaut
Gugulethu Nkala
Mathias Kiefer
Sikhumbuzo Masina
Dennis Malihase
Masilo Ramafemo

## Slide 5: Fast Ion Conductors
Aka solid electrolytes
Solids in which ions are highly mobile.
Used in supercapacitors, batteries, fuel cells and chemical sensors.

## Slide 6: Fuel Cells
Anode
Electrolyte
Cathode
A device that converts the chemical energy from a fuel into electricity through a chemical reaction.
Needs a continuous source of fuel (ie different from a battery)
First ones invented in 1802. (Davy), then Grove cell in 1838
SOFC
Consists of :
AFC
DMFC
PEMFC
MCFC
SOFC
Fuel Cell Types :

## Slide 7
Fuel cell stack
2H2 + 2O2 –  2H2O + 4e–
O2 + 4e–  2O2–
Fuel flexible
High oxide conductor
Electronic insulator
Solid oxide fuel cells
The Focus

## Slide 8
Nissan SOFC driven vehicle
Used mainly in stationary energy conversion
Why SOFCs?

## Slide 9: Extending the idea
RSOFC !

## Slide 10: Material requirements:
Desirable characteristics for electrolyte, cathode and anode materials |  | 
Cathode / Air | Electrolyte | Anode / Fuel
Electronic conductor | Electronic Insulator | Electronic conductor
Ionic Conductor | Ionic Conductor | Ionic Conductor
Porous | Gas tight | Porous
Stable in Air at high T | Stable in air and fuel at high T | Stable in fuel at high T, ideally also stable in air at high T
No reaction with other cell components | No reaction with other cell components | No reaction with other cell components
Matched coefficient of thermal expansion | Matched coefficient of thermal expansion | Matched coefficient of thermal expansion
Catalyse O2 reduction |  | Catalyse H2 oxidation
 |  | Catalyse fuel processing if needed

## Slide 11: Materials generally used:
Electrolyte:
YSZ – Yttrium Stabilized Zirconia
CaSZ
SDC – Samarium doped Ceria
Fuel Electrodes
Mostly Ni-cermet
Eg Ni/YSZ
Oxygen Electrodes
Often Perovskites
Eg LSM – La1-xSrxMnO3-δ
Oxide Ionic conductivities

## Slide 12
Ceria based materials – Popular LT-SOFC Electrolyte Candidates. (Artini, 2018 – “Puzzling Tangle” Review)
Structural map of phases occurring in RE-doped ceria systems:
Synthetic method impacts on
Lattice Parameter
Few systematic studies reported
Conductivity
Density
Structure / Phase
Characterisation method also NB
PDF Studies / Local Structure
Ce1‑xGdxO2‑x/2 (Coduri, 2013; Scavini, 2012))
CeO2−Sm2O3 (Coduri, 2018)
Ce1−xYxO2−x/2 (Coduri, 2013)
Values of CTE at 1073 K for Sm and Gd-35doped ceria and at 1473 K for Nd-doped

## Slide 13: Our synthetic Capability
Various Mixed Metal Oxides
  Spinel, A2BO4
  Perovskite, ABO3
  Flourite, ABO4
  Defect Flourite / Pyrochlore, A2B2O7
Doped / Solid Solution variants.
  Doped Bi2O3
  Doped Ce2O
Ceramic / Shake-n-Bake
Sol-Gel / Chemie Douce
Mechanochemical
Hydrothermal
For A2B2O7
  B = Zr
  B = Ti
  B = Hf
DOI : 10.1080/24701556.2017.1326140
  B = Pb
So far Prepared a sample library with > 300 permutations

## Slide 14
 O2- conducting ceramics
Yttrium stabilised zirconia (YSZ) most common
  Problem: Operates at high temperatures (generally >800 C)
Improve conductivity of solid electrolytes at lower temperatures
 Our Focus : stabilised bismuth oxide based-materials
Electrolyte materials
Highest known oxide conductor (~100× more conductive than YSZ at the same temp)
Conductive at lower temperatures (500-650C)
Need to stabilise conductive phase to room temperature
Stability problems on thermal cycling
Stability problems in reducing atmospheres (becomes electronically conducting)
PROs
CONs

## Slide 15
824
729
650
629
500
330
 phase
fcc
 phase
fcc
 phase
fcc
 phase
monoclinic
 phase
tetragonal
 phase
bcc
 phase
monoclinic
 phase
or
 phase
may persist
Liquid




3 × 10-4
2 × 10-3
5 × 10-3
1
Conductivity at 600 C /-1 cm-1
Ionic conductor
Electronic conductor
Some ionic >580 C
Solid State Ionics 21 (1986) 183
Arrhenius constant increases with the fraction of vacant anion sites.
Ionic conductivity is strongly temperature dependent:
Phases of Bi2O3

## Slide 16
ions assume fcc lattice
Only 75% of these sites are occupied
Defect fluorite structure ()
Bi3+
O2-
ions occupy the tetrahedral sites
Battle model:
six oxygen atoms distributed at the 8c and 32f sites
(Neutron diffraction data)
Gattow model:
six oxygen atoms distributed at 8c sites
Structure of -Bi2O3
Chemical Physics Letters 378 (2003) 395

## Slide 17
But -Bi2O3 only exists between ~729 - 824C
must be stabilised at room temperature  done by doping
often isovalent dopants are used, but aliovalent ions have also been used
High O2- conductivity
vacant O-sites
3D structure and highly symmetric
low activation energy barrier for O2- ion to move
long Bi-O bond lengths
highly polarisable Bi3+ which has a lone pair of electrons
In the case of zirconia, dopants need to have a lower valence than Zr4+ to introduce vacant sites at the oxygen positions.
These vacancies are inherent in the -Bi2O3 structure.
Properties of -Bi2O3

## Slide 18
Use the citrate gelation method for synthesis.
Metal ions complexed by citrate to form a coordination network.
Ensures that nucleation sites are evenly dispersed and numerous, producing small crystallite sizes.
Citrate is combusted (at 450 C) to form the mixed metal oxides.
For ternary and quaternary systems, the matrix ensures the different metals remain mixed on an atomic scale.
Synthetic strategy
Both the monoclinic
 phase

## Slide 19
Y3+ substitution – in-situ VT-Raman Spectroscopy
23C
510C
170C
340C
Back to
30C
850C
680C
27.5% Y3+
F2g 
 - fcc ()
The sample decreases in volume visibly on heating when the dominant phase becomes fcc
heating

## Slide 20
Y3+ substitution – in-situ VT-High Resolution XRD
17.5% Y3+
80C
210C
300C
390C
470C
550C
590C
630C
660C
700C
735C
770C
Radiation wavelength 0.035445 nm
ESRF - ID22
Measurement temperature
Peak shifts due to thermal volume change

## Slide 21
Y3+ substitution – in-situ VT-High Resolution XRD
700C
735C
770C
17.5% Y3+
Set temperature 900 C
Lower intensities due to decrease in sample volume

## Slide 22
 |  | Sintering Temperature /C |  |  |  |  | 
 |  | 450 | 550 | 650 | 750 | 850 | 950
Mole % Y3+ | 8.75 |  + |  + | ++C + |  | +C + | A
 | 10.0 | +C + | ++C + |  + |  | +C + | A
 | 12.5 | ++C + | ++C + |  + |  |  | +C +
 | 13.75 | +C + |  |  |  |  | +C +
 | 22.5 | +C + |  |  |  |  | A
 | 28.75 | +C + |  |  |  |  | 
 - tetragonal ()
 - fcc ()
A - amorphous
C - mix of cubic phases
Y3+ substitution – Summary of observations
Higher % substitution  -phase easier to stabilise
 - monoclinic

## Slide 23
Testing thermal stability (Y3+ substitution – 32.5%)
Samples obtained after annealing at 950C * were left at 650C for various times.
*
650C for 96 hr
650C for 24 hr
Typical for SOFC operation using this electrolyte
Phase | * | 650C for 24 hr | 650C for 96 hr | 650C for 117 hr
 (m) | 100 % | 99 % | 91 % | 63 %
 (b2) | 0 % | 1 % | 9 % | 37 %
Phase | * | 650C for 24 hr | 650C for 96 hr | 650C for 117 hr
 | 100 % | 99 % | 91 % | 63 %
 | 0 % | 1 % | 9 % | 37 %
(21c)
32.5% Y3+

## Slide 24
Co-doping
6% Dy3+ + 6% W6+
8% Dy3+ + 4% W6+
8% Dy3+ + 3% Er3 + 1% W6+
By co- or triple-doping smaller concentrations of substituents are needed to stabilise the -phase.
The lower the total dopant concentration, the higher the conductivity.
Total M = 12%

## Slide 25
Co-doping : (Dy2O3)0.08(Er2O3)0.03(WO3)0.01(Bi2O3)0.88
Arrhenius plots of the bulk conductivities for both the heating and cooling cycles. The activation energies (Ea) are indicated for the linear regions.
Plot of the unit cell length as a function of temperature. The thermal expansion coefficients () for the linear regions are also shown for the heating cycle. (Assuming FCC)
the δ-phase (Fm-3m) was converted to a mixture of the δ-phase with a primitive cubic phase (Pn-3m) and a cubic superstructure (Fm-3).
no apparent corresponding phase change on cooling, instead with some peak broadening from 510°C (except for the (hhh) reflections. Could this be due to the formation of an additional tetragonal phase which also reduced the lattice parameter?

## Slide 26
Dopants considered so far:
Prepared a sample library with > 300 permutations

## Slide 28: What determines a materials properties and performance in an electrochemical device?

## Slide 35: Total Scattering
“Conventional” powder diffraction data analysis is insufficient or fails in particular for non crystalline materials (disorder, defects) and nanomaterials (short structural coherence length, broad Bragg peaks)
PD patterns of complex materials often shows diffuse scattering smeared in the reciprocal under the Bragg peaks.
FT of the total powder diffraction data ( Bragg + diffuse ) gives the PDF.
Carbon buckyballs

## Slide 37: Schematic representation of the PDF
5.11Å
4.92Å
4.26Å
3.76Å
2.84Å
2.46Å
1.42Å
Pair distribution function (PDF) gives the probability of finding a neighbor atom at a distance “r” from a given atom.
Q = 4π Sin(θ)/λ

## Slide 38: Nd2Ru2O7
Gaultois et al, J. Phys.: Condens. Matter 25 (2013) 186004
7% Antisite defect.

## Slide 39: Ho2Ti2O7 , Ho2Zr2O7
Shamblin et al., Nature, Materials. (2016)
Heavy / Large Ho on A-site biases towards B-site disorder

## Slide 40
Shamblin et al., Nature, Materials. (2016)

## Slide 41: Our Synchrotron Measurements - 1
Various A2B2O7
Some Bi2O3
A2B2O7 - PDF
Bi2O3 , YSB, HR-XRD
RT - Only
VT, RT to 1000 C
Beamtime – ID22 HR-XRD, PDF, VT
60 samples, 3 days

## Slide 43: Our Synchrotron Measurements - 2
Various Doped Bi2O3
Some battery materials
Doped Bi2O3
RT - Only
VT, RT to ~850 C
Beamtime – ID-28-1 XPDF XRD + PDF, VT
`160 samples, 3 days

## Slide 44: 27.5YSB

## Slide 45: 24Y1AlSB

## Slide 46
In the Pipeline
~300 composition in our materials library
Complete Data analysis & characterisation.
Stability & Formation studies
7 PG students and 1 PDF
Proof of concept devices
Reproducibility studies
High Res & anomalous XRD studies
XAS studies
To be continued……..

## Slide 47
Students:
Mathias Kiefer
Sikhumbuzo Masina
Dennis Malihase
Masilo Ramafemo
Acknowledgements
Collaborators:
Dr Caren Billing
Dr Tumaini Mkwizu (PDF)
Dr Rudolph Erasmus
Dr Stuart Miller
UCT: Dr Wilson Mogodi
SSRL: Dr Kevin Stone
NSLS-II : Dr Daniel Olds

## Slide 49: Thank You

## Slide 50: Pasteur's Quadrant
Fundamental research aimed solving important applied problems
Fundamental research aimed solving important applied problems
Fundamental research aimed solving important applied problems

## Slide 51: Gigaton challenges and Elemental Abundance

## Slide 52
12D4.5E1.5WSB