## Slide 1: The Search for an Improved SOFC Electrolyte Material: Stabilizing the Fm3̅m Phase of Bismuth Oxide to Lower Temperatures
A presentation by Mathias A. Kiefer

## Slide 2: The (not-so-great) State of the World
Global Population Growth
Global Demand for Energy

## Slide 3: Satisfying the Energy Demand

## Slide 4: …but at what cost?

## Slide 5: Plenty Alternatives Are Available
Polymer Electrolyte Membrane (PEM) Fuel Cell
Alkaline Fuel Cell (AFC)
Molten Carbonate Fuel Cell (MCFC)
Solid Oxide Fuel Cell (SOFC)

## Slide 6: SOFC Working Principle
Air
H2
Electrolyte
Anode
Cathode
O2
O2
O2
H2
H2
O2-
O2-
O2-
O2-
O2-
H2O
O2-
H2O
H2
H2

## Slide 7: Advantages of SOFCs
+ Fuel Flexibility
H2, bio-ethanol, CH4, etc
+ Excellent Efficiencies
Up to 85%
+ Reduced emissions
Dependent on fuel
+ All solid state device
No scary liquids!
Ragone Plot

## Slide 8: SOFCs sound great but…
High operating temperature 500 – 1000 oC
Dictated by the electrolyte material
Knock-on effects:
Chemical (Phase) Degradation
Thermal expansion incongruities
Overall: Very Limited lifespans (<10000 hours)
Why haven’t we seen any SOFCs yet? – Material Limitations!

## Slide 9: Currently used electrolyte: 8YSZ
High ionic conductivity
Low(er) thermal expansion
High phase stability
BUT: High temperatures needed – material limitation
Overall: Device lifespan limitations

## Slide 10: What options are available?
‘Why aren’t doped bismuth oxides used commercially?’
10

## Slide 11: Bi2O3 as an alternative
Bi3+
O2-
SG: Fm3̅m (#225)

## Slide 12: We need an improved electrolyte
12
High Phase Stability and Purity
High Oxide ion conduction at lower temperatures
Low thermal expansion

## Slide 13: Stabilizing the delta phase to lower temperatures – ‘doping’ approaches
Y3+/Bi3+
O2-

## Slide 14: Successful … BUT there are problems
12 months
Problem #1: Aging phenomenon

## Slide 15
Lab data
NSLS-II data
Problem #2: Phase purity

## Slide 16
Lab data
NSLS-II data
Phase purity continued

## Slide 17
Synchrotron data used to unravel anomaly
Problem #3: Anomalous conductivity data

## Slide 18: A new hope: PDF measurements
Local structure changes = anomalous cond.

## Slide 19: The Need for synchrotron data
Material challenges: High resolution Bragg and PDF data is needed
ID-28-1 at NSLS-II 
I11 at DLS (fingers crossed!)

## Slide 20: A word of thanks

## Slide 21: Thank You/Merci! Any questions, comments or suggestions?