## Slide 1: Superionic Conductors For Solid Oxide Fuel Cells: Probing the Local And Average Structure of the Enigmatic Bismuth Oxide and Its Chemical Derivatives
Name: Sikhumbuzo Masina
Supervisors: Prof. D. G Billing
Dr C. Billing

## Slide 2
https://www.doitpoms.ac.uk/tlplib/fuel-cells/high_temp_sofc.php, Dziurdzia, B., Magonski, Z. and Jankowski, H., 2016. Commercialisation of Solid Oxide Fuel Cells-opportunities and forecasts. In IOP Conference Series: Materials Science and Engineering (Vol. 104, No. 1, p. 012020). IOP Publishing.
SOLID OXIDE FUEL CELL COMPONENTS
Over 60% efficient in stand alone configuration
Over 80% efficient in combined heat and power configuration.

## Slide 3
Synthesis of mesoporous nanocomposites for their application in solid oxide electrolysers cells: microstructural and electrochemical characterization M. Torrell, L. Almar, A. Morata and A. Taranc´on* DOI: 10.1039/c5fd00035a
DEGRADATION OF CELL COMPONENTS

## Slide 4: THE DELTA PHASE
Defect fluorite delta phase (Fm-3m) has the highest conductivity for any oxide ion conductor ever reported.
Unfortunately it’s only stable within a narrow range 730-824 °C
Bi3+
O2-
Vacancy

## Slide 5: Ambient Temperature XRD
(Bi2O3)0.88 (Dy2O3)0.08 (WO3)0.04 (8D4WSB)
(Bi2O3)0.88 (Dy2O3)0.08 (Er2O3)0.03 (WO3)0.01 (8D3E1WSB)
(Bi2O3)0.88 (Dy2O3)0.08 (Er2O3)0.04 (8D4ESB)

## Slide 6: VT-ELECTROCHEMICAL IMPENDANCE SPECTROSCOPY
σ700 °C = 0.227 S/cm
σ500 °C = 0.00033 S/cm
Lit σ500 °C
Lit σ700 °C
Literature values sourced from: Effect of total dopant concentration and dopant ratio on conductivity of (DyO1.5)x–(WO3)y–(BiO1.5)1-x-y by Doh Won Jung, Keith L. Duncan, Eric D. Wachsman

## Slide 7: Vt-XRD
8D3E1WSB

## Slide 8
8D4ESB-NO W6+

## Slide 9: vt-Raman Spectroscopy

## Slide 10
Lab XRD Data vs Synchrotron XRD data
8D3E1WSB
8D3E1WSB

## Slide 11: Phase Stability Test
100h
100h
500 °C

## Slide 12: Conclusion and Future work
There’s overwhelming evidence for a link between average structure and conductivity.
What role is the local structure playing on the conductivity?
The rapid acquisition pair distribution function (RAPDF) technique will be used to probe the local structure.
EXAFS will also be used to compliment the PDF and probe the oxidation states of the impurity cations.

## Slide 13: Acknowlegements
13

## Slide 14: Thank you very much, Questions are most welcome