## Slide 1
Bio-mimicry of photonic multi-scaled architectures of butterfly wing
1. AIM
● Investigate the contributing factor of blackness on wing eyespot of Caligo memnon butterfly”.
J. Sackey1-2 , M. Maaza1-2
(1): UNESCO UNISA AFRICA Chair in Nano, South Africa. (2): NANOAFNET, iThemba LABS, South-Africa,
jsackeyunisa@gmail.com
4. RESULTS & DISCUSSION
Type equation here.
4.1. SEM
● In fig.1. SEM is made of almost parallel ridges separated by crossribs. This period is changing from place to place. crossribs are not fully parallel nor perpendicular to the ridges. both the shape and position of the crossribs and the ridges possess some degree of disorder.
● As shown in Fig.2, the autocorrelation function unveils beautiful structures of parallel periodic lines perpendicular x to whose intensities are modulated along these lines (// y ). Observation of so many lines is the signature of a long range order. On the contrary, the observation of a few sharp peaks along y is a clear indication that the crossribs are short range ordered
● The periodic order is 10 times more correlated along x than along y. The background (A and C parameters) were constant along both directions.
● The 2-D Fourier pattern exhibits clear features along lines, which are parallel to the ones of the ridges and crossribs As noticed, the features observed along y are sharp and equally spaced while the ones along x are significantly broad. Once again this is in full agreement with the fact that the ridges are long range ordered while the crossribs are only organized at short range respectively
4.2. Optical Analysis
●Fig.5 shows ~ 30% absorption increase in the IR range when the wing scale was immersed in toluene. The spectra indicate melanin pigment and thus contribution from the nanostructure is predominating in the near IR. Similar to Vukusic, et al. observations on single scales the ridge-cross-rib hybrid nanostructures found on the butterfly eyespot scatters incident light.
4.2. Conclusion
Thus both the nanostructure and the melanin pigment found on the eyespot of the Caligo Memnon, contribute to optical absorption and the blackness of the wing eyespot.
Fig.1
Fig.2
Fig.4
Fig.5
Inner ring of the Ocellus (black section)
● Theoretical approaches
Autocorrelation function and Fourier transform
Periodic ridges
crossribs
a
b
Small features on the ridges
Fig.3
2. Background
●In recent times, scientist have gain much interest in the study and biomimic nature’s abundant systems for various innovative purposes ranging from the designs of aircraft inspired by birds and bat, through to trends on tries inspired by toe pads of tree frogs and selective colors and quality digital display inspired by the photonic properties of butterfly wings
●Studies on butterflies wings have proven to be multi-functional composed of multi-scale periodicity within nano/micro structures suitable for heat regulation & hence suitable for selective solar absorber applications. More accurately, the black wings of butterfly absorb significant light and reflect very little.
Fig.4