## Slide 1: Fast neutron transmission spectroscopy for the non-destructive analysis of concrete
Naledi Segale
Tanya Hutton, Andy Buffler & Sizwe Mhlongo
SAIP2023

## Slide 2: Concrete in nuclear power plants
… is used for:
structural support
containment
radiation shielding
… and is exposed to:
cyclic loadings
radiation
extremely varying temperatures
… induces concrete degradation over time, particularly
with respect to water (hydrogen) content

## Slide 3: Ordinary concrete composition
Constituent | Percentage by mass (%)
Large aggregate (stone) | 61
Small aggregate (sand) | 11
Portland cement | 13
Water | 15
Additives, voids, variations in the mixing and curing increase
the complexity of the composition of concrete

## Slide 4: Koeberg NPP
2 x 970 MW PWR units
Commissioned in 1980s and its license expires in July 2024
The plan is to extend its life by 20 more years, overseen by National Nuclear Regulator
The non-destructive testing of existing concrete structures is crucial to the plant life extension
Koeberg, Eskom

## Slide 5: Fast Neutron Transmission Spectroscopy
Effective removal
cross section
Energy dependent cross section
is unique to each element
Mass ratio of component k

## Slide 6: Aim
To build a repository of elemental response functions, thus determine the elemental composition of aging concrete used in nuclear facilities. Starting off with sand, an integral part of any concrete as an example case
Measure for
Simulate for in FLUKA
Use XRF data to reconstruct for sand and compare to measured and simulated data
Objectives
Validate FLUKA simulations in the context of neutron transmission

## Slide 7: Fast neutron facility at UCT
Neutron energy (MeV)
Fluence rate (cm-2s-1)
 | STNG | AmBe
Type | Accelerator | Radioisotopic
Reaction | t(d, n)a | 9Be(a, n)12C*
Energy | 14.1 MeV | < 11 MeV
Yield | 108 s-1 | 107 s-1

## Slide 8
220 GBq 241Am-9Be radioisotopic source
Neutron beams produced with HDPE collimator (∅ 0.8 cm)
Neutron fluence rates of 40 cm-2 s-1 at 1.50 m
neutron
source
sample
detector
analysis

## Slide 9
neutron
source
sample
detector
analysis
Sample | g cm-3]
Sand | 1.53 ± 0.03
SiO2 | 1.26 ± 0.03
CaCO3 | 0.693 ± 0.029
Sample | 
Sand | 1.53 ± 0.03
SiO2 | 1.26 ± 0.03
CaCO3 | 0.693 ± 0.029
8
Sample container has dimensions of 6.2 (b) 6.6 (t) 10.0 cm

## Slide 10
EJ-301 reference detector
2”x 2” organic liquid scintillator
Well characterised
Pulse shape discrimination to exclude gamma rays
Digital data acquisition and pulse processing (QtDAQ)
neutron
source
sample
detector
analysis
neutrons

## Slide 11: Spectrum unfolding
Measured pulse neutron height spectrum…
… is unfolded (GRAVEL) using detector response functions…
… to produce neutron energy spectrum

## Slide 12: Measurements with sand
Neutron energy
unfolded
with GRAVEL
Energy dependent
removal cross sections

## Slide 13: Measured sand
Sand is made up of 78.5 % SiO2 and 18.6 % CaCO3 with the remaining 2.9 % consisting of other oxides

## Slide 14: FLUKA simulations
Simulate the energy dependent neutron fluence transmitted through sand,
Source:
241Am-9Be
neutron
source
Sample:
t= 10.0 cm, r= 5.0 cm
Detector:
Energy dependent
neutron fluence
Sample | (g cm-3)
SiO2 | 1.42
CaCO3 | 0.372
Sample | 
SiO2 | 1.42
CaCO3 | 0.372

## Slide 15: Simulated
Preliminary simulation results for all three samples.

## Slide 16: Simulated sand
Known ratios were applied to simulated SiO2 and CaCO3 .

## Slide 17: Results
Overall shape is well matched between simulation and measurement.
Around the 3 MeV region, the enhancement due to O is consistent in
simulated and measured data.
Broadened features in measured data due to measurement process.

## Slide 18: Summary
Non-destructive testing of concrete is crucial to nuclear industry.
Fast neutron transmission measurements for sand and its constituents were made.
Effective removal cross sections determined via measurement and simulation.
Preliminary investigations show good agreement between measured and simulated removal cross sections.

## Slide 19: Next steps
More experimental validation is required to investigate the energy broadening in measured vs. simulated data.
Build a repository of elemental response functions.
Investigate elemental unfolding to determine mass ratios for known and unknown samples.

## Slide 20: Thank you