## Slide 1: Temperature and Moisture Triggered Crystallization of Triple Cation-Mixed Halide Perovskite Cells to Reduce Phase Segregations
Miller Shatsala and Celline Awino
Department of Physics
Masinde Muliro University of Science and Technology, Kakamega, Kenya

## Slide 3
Google source

## Slide 4
Zhang, T., Wang, M., & Yang, H. (2018). Energies, 11(11), 3157.
PEROVSKITE USES
Sensors and catalyst electrodes
fuel cells
solar cells
Lasers
memory devices
Spintronics
ISSUES
INSTABILITY

## Slide 5
Perovskites
Kojima et al., J. Am. Chem.Soc. 131 (2009) 6050
Stranks et al., Science 342 (2014) 341
Processing from salt solutions
CH3NH3PbI3: mature, most prominent
Eg = 1.55 eV, long diffusion length
CH3NH3Pb(IxBr1-x)3: tunability of Eg
Cs(MA,FA)Pb(IxBr1-x)3: increase of stability
ABX3
A: (CH3NH3)+, Cs+, (CH3(NH2)2)+,…
B: Pb2+, Sn2+,…
X: I-, Br-, Cl-
MA: methyl ammonium
FA: formamidinium

## Slide 6: Motivation
Perovskite crystallization has not been understood well to date.
Over emphasis on their efficiencies.
Difficulty in measuring the critical nucleus sizes in the range of 100 to 1000 atoms.
Synchrotron radiation-based X-ray techniques allow structural characterization providing valuable information about the inner film morphology.

## Slide 7
Sizes, shapes, distances, and correlations of particles are determined from these measurements.
These parameters are fundamental in understanding the process of nucleation and growth.
We seek to address the influence of heat stress and moisture probing on the crystallization kinetics of triple cation-mixed halide perovskite cells.
Using in situ and static GIWAXS/GISAXS, Micro-Diffraction and Optical microscopy through photoluminescence techniques.

## Slide 8: Perovskite preparation
Sample Preparation:
CsI, MAI & FAI and PbI2 & PbBr2 in stoichiometric ratios
dissolved in 800 µl of DMF and 200 µl dimethyl sulfoxide (DMSO) in ratio of 4:1
Mixed overnight at 60° C in a nitrogen filled glovebox.
MMUST – MRL Glove Box
Precursor Solution

## Slide 9
100ul of precursor solution spin coated onto a substrate in two steps 30s.
Anti-solvent introduced after 20s of spin coating
Annealing at 1500C for 15 minutes on a hot plate with 500 rpm..
Hot plate
Spin Coater
ITO substrate
Precursor dropping
Perovskite film
Reversible

## Slide 11
7.3.3 GIWAXS/GISAXS
Beamline 7.3.3 is a GISAXS/GIWAXS beamline, covering a wide q range (0.004 - 3 Å−1) and length scale (2 - 1500 angstrom)

## Slide 12
12.3.2. Microdiffraction

## Slide 13
Sample Testing
custom-built Multi-Modal Spin Coater with auxiliary inputs.
Sample viewed from the computer interface
MMSC mounted on the stage
Computer Interface
Humidity Controller

## Slide 14: Results
Diffraction characteristics of 2T films.
GIWAXS spectra of 2T films based on precursor solutions prepared by different solvent conditions: GBL, GBL/MeOH, GBL/DMSO, GBL/DMSO/MeOH.
Coffey, A. H. et al. (2023). Advanced Energy Materials, 13(33), 2201501.

## Slide 15
Liu, Y. et al. (2019). Science advances, 5(6), 2543.

## Slide 16: Degradation of perovskite samples
Fresh samples Degraded samples

## Slide 19
Chenhui Zhu and Aidan Coffey – Advanced Light Source (LBNL)
Carolin Sutter-Fellow- Molecular Foundary (LBNL)
Prof. Husein Golicha and Dr. Maxwell Mageto - MMUST
Acknowledgements

## Slide 20: Thank You.