## Slide 1: Synchrotron Techniques on Moisture Triggered Crystallization of Triple Cation Perovskite to Elucidate Phase Progression Nucleation
Miller Shatsala
Advanced Light Source, Lawrence Berkeley National Laboratory, Berkeley,CA,USA.
Department of Physics, Masinde Muliro University of Science and Technology, Kakamega, Kenya

## Slide 2
Google source
Current: LAAAMP FAST award & ALS fellowship

## Slide 3
Home: Masinde Muliro University of Science and Technology

## Slide 4
PEROVSKITE USES
Sensors and catalyst electrodes
fuel cells
solar cells
Lasers
memory devices
Spintronics
ISSUES
INSTABILITY
Zhang, T., Wang, M., & Yang, H. (2018). Energies, 11(11), 3157.
Motivation

## Slide 5
Perovskites
ABX3
A: (CH3NH3)+, Cs+, (CH3(NH2)2)+,…
B: Pb2+, Sn2+,…
X: I-, Br-, Cl-
MA: methyl ammonium
FA: formamidinium
Processing from salt solutions
CH3NH3PbI3: mature, most prominent
Eg = 1.55 eV, long diffusion length
CH3NH3Pb(IxBr1-x)3: tunability of Eg
Cs(MA,FA)Pb(IxBr1-x)3: increase of stability
Kojima et al., J. Am. Chem.Soc. 131 (2009) 6050
Stranks et al., Science 342 (2014) 341

## Slide 6
100ul of precursor solution spin coated onto a substrate in two steps 30s.
Anti-solvent introduced after 20s of spin coating (CB/EA)
Annealing at 1500C for 15 minutes on a hot plate with 500 rpm..
Hot plate
Spin Coater
ITO substrate
Precursor dropping
Perovskite film
Reversible
Sample preparation

## Slide 7
Beamline Technique
custom-built Multi-Modal Spin Coater with auxiliary inputs.
Sample viewed from the computer interface
MMSC mounted on the stage
Computer Interface
Humidity Controller

## Slide 8: Micro-difraction Results
Beamline 12.3.2 Advanced Light Source
Figure 1| Micro-diffraction peaks for 3-CAT dissolved in both EA and CB. Sharp peaks of the perovskite phase (100) with small peaks of crystal planes of (220), (310) and (314) corresponding to plane angles of 14.10, 28.50, 34.10 and 43.60 respectively.
3-CAT Peak identificatication (CB/EA)

## Slide 9: Micro-difraction Results
Beamline 12.3.2 Advanced Light Source
Figure 2| Micro-diffraction synchrotron maps for films treated with different anti-solvents (a) MAPI treated with CB and the corresponding 1D peaks adjacent. (b) MAPI treated with EA with the adjacent 1D peaks.
MAPI Peak identificatication (CB/EA)

## Slide 10: GIWAXS Results
Beamline 7.3.3 Advanced Light Source
Figure 3| GIWAXS maps of triple cation (3-CAT) with varying cesium concentration in triple cation at (a) 0% Cs ; (b) 5% Cs; (c) 10% Cs; (d) 15% Cs and ( e ) 20%
Cs variation for 3-CAT

## Slide 11: GIWAXS Results
Beamline 7.3.3 Advanced Light Source
Figure 4| GIWAXS maps of triple cation (3-CAT) upon exposure to moisture of relative humidity for (a) 0% (b) 11 % (c) 44 % (d) 88 % (e) 103% and (f) 111 %. The real perovskite films with respective humidities are shown.
Humidity probing for 3-CAT

## Slide 12: GIWAXS Results
Beamline 7.3.3 Advanced Light Source
Figure 5| GIWAXS of triple cation with 5% Cs in q-space for RH of 111%
1D profie for humidity

## Slide 13: GIWAXS Results
Beamline 7.3.3 Advanced Light Source
Figure 6| GIWAXS maps of MAPI when exposed to relative humidity (RH) of (a) 0% % (b) 32%; (c) 51% (d) 82% (e) 91% and (f) 102%
Humidity probing for MAPI

## Slide 14: GIWAXS Results
Beamline 7.3.3 Advanced Light Source
Figure 7|GIWAXS peaks of MAPI when exposed to 10% relative humidity (RH) for 10s with a slight variation of scanning points ranging from 0.100mm to 0.500mm starting from the edge of the sample.
1D profile for MAPI humidity

## Slide 15
Prof. Sekazi Mtingwa- LAAAMP
Ashley White - Deputy Director communications- ALS
Chenhui Zhu and Nobumichi Tamura – Advanced Light Source (LBNL)
Carolin Sutter-Fellow- Molecular Foundary (LBNL)
Dr. Celine Awino -MMUST
Prof. Husein Golicha, Dr. Maxwell Mageto - MMUST
Acknowledgements

## Slide 16
Publication
AfLS Outreach for potential users
Omolara Bakare
Virgia Tech
Tianying Liu
University of Boston
Nushrat Naushin
UC Davis
Nicole Taylor
Havard University
Nadja Maldonado Luna
UC San Francisco

## Slide 17: Thank You.
Any Questions?