## Slide 1: Harnessing Metal Organic Frameworks for CO2 Conversion: Unlocking New Pathways for Formate Synthesis .
Dr Piwai Tshuma
Midlands State University
Department of Chemical Sciences

## Slide 2
Introduction

## Slide 3: Introduction
Challenge in CO2 utilisation
Highly active catalysts required
Homogeneous catalysts
Heterogeneous catalyst

## Slide 4: Metal Organic frameworks (MOFs)
Ye J, Johnson JK. ACS Catal. 2015, 10, 6219-6229
Abelegi et al. American Journal of Environmental Protection, 2017, 5, 61-67

## Slide 5: Methodology
Pd@Mg:JMS-2 and Pd@Mn:JMS-2
C1

## Slide 6
Structural description
Void volume 43.8% and 46.6% for Pd@Mg:JMS-2 and Pd@Mn:JMS-2 respectively
 | Pd@MgJMS-2 | Pd@MnJMS-2
Crystal system | monoclinic | monoclinic
Space group | C2/c | C2/c
Volume(Å3) | 4596.9 | 4742.3
a(Å) | 27.22 | 27.53
b(Å) | 7.76 | 7.86
c(Å) | 22.32 | 22.47
β/° | 102.76 | 102.68
Goof | 1.071 | 1.035
z | 8 | 8

## Slide 7
Thermal, PXRD and FTIR analysis

## Slide 8
Entry | Catalyst | Base | Temp(°C) | Pressure (bars) (CO2:H2) | TON | TOF
1 | Pd@Mn:JMS-2a | Et3N | 90 | 40 (1:3) | 2448 | 102
2 | Pd@Mn:JMS-2a | KOH | 90 | 40 (1:3) | 4896 | 204
3 | Pd@Mn:JMS-2a | NaHCO3 | 90 | 40 (1:3) | 3672 | 153
4 | Pd@Mn:JMS-2a | K2CO3 | 90 | 40 (1:3) | 484 | 121
5 | Pd@Mn:JMS-2a | None | 90 | 40 (1:3) | 0 | 0
6 | None | KOH | 90 | 40 (1:3) | 0 | 0
7 | Pd@Mn:JMS-2a | KOH | 90 | 20 (1:1) | 1752 | 73
8 | Pd@Mn:JMS-2a | KOH | 90 | 30 (1:2) | 2880 | 120
9 | Pd@Mn:JMS-2a | KOH | 90 | 50 (1:4) | 7488 | 312
10 | Pd@Mn:JMS-2a | KOH | 90 | 40 (0:4) | 0 | 0
11 | Pd@Mn:JMS-2a | KOH | 90 | 10 (1:0) | 0 | 0
12 | Pd@Mn:JMS-2a | KOH | 100 | 50 (1:4) | 9816 | 409
13 | Pd@Mn:JMS-2a | KOH | 100 | 50 (1:4) | 7272 | 303
14 | C1 | KOH | 100 | 50 (1:4) | 4080 | 170
Catalysis Studies
Conditions: Time (24 hours), ethanol (8 mL) and base (5 mmol) and TONs are based on Pd (0.46 µmol). The yield based on 1H NMR analysis using acetone as an internal standard.

## Slide 9: Recyclability Studies

## Slide 10
Recyclability Studies

## Slide 11: Conclusion
The functionalised MOFs, Pd@Mn:JMS-2a, Pd@Mg:JMS-2a displayed excellent catalytic hydrogenation of CO2 to formate under relatively mild conditions.
Catalytic performance of homogeneous catalysts can be improved by incorporating them in MOFs as organic linkers bearing catalytic sites.
Future work
Testing the catalysts in a packed bed flow reactor-a crucial step in scaling up the process for industrial applications.

## Slide 12: Acknowledgements
Prof. Gift Mehlana
Prof Banothile Makhubela
Dr N Bingwa
Dr Hong Su
Organometallic Group
Gift Mehlana Research Group