## Slide 1
Debye Institute for
Nanomaterials Science
Peter Ngene
Materials Chemistry and Catalysis, Debye Institute for Nanomaterials Science, Utrecht University.
AFLS-AfPS conference 2024
XRS Studies on Nanocomposite Energy Storage Materials
Notes: Resume : Complex metal hydrides are a promising class of solid-state electrolytes for future generation all-solid-state batteries. In this presentation I will share information about the research in this field in our group over the past five years, most notably discussing: * improved conductivity in nanocomposites, by combining with high surface area/porous oxides ("interface engineering") * design rules how to maximum the room temperature conductivity * synergy between anion replacement and nanocomposites * progress towards practical room temperature all-solid-state batteries based on these electrolytes references: Suwarno et al, J. Phys Chem C 121 (2017) 4197 Zettl et al. J Phys Chem C 124 (2020), 2806 Gulino et al, ACS Appl. Ener. Mater. 121 (2017), 4941 de Kort et al, J. Alloys Comp. 901 (2022) 163474

## Slide 2: Overview
Motivation (Energy transition and energy storage)
Nanocomposites for Reversible Hydrogen storage
Nanocomposites solid electrolytes for batteries
Conclusions and outlook
Notes: changing focus, although classic fields still important, new fields emerging

## Slide 3
Energy and Economic development
Coal
Industrial revolution and economic development spurred by availability of energy resources (coal)

## Slide 4
Crude oil
Natural gas
Coal
Energy and Economic development

## Slide 5
Energy and Economic development
The GDP per capita proportional to energy consumption
Increasing energy demand vs depleting oil reserves, pollution/global warming
David S. Ginley and David Cahen., Fundamentals of Materials for Energy and Environmental Sustainability

## Slide 6: Energy Transition
www.simplerenewable.com
Crude oil
Natural gas
Coal

## Slide 7: Energy from renewable resources
Growth is mostly driven by concern about climate change, decreasing cost of PV cells
Cost
CAGR: Compound annual growth rate

## Slide 8
Energy storage: A challenge for renewables
Electricity from wind (California)
needed
The transition to renewable energy requires suitable energy storage
nacht
morgen
middag
avond
July
August
September
Electricity needed
wind electricity

## Slide 9
Energy storage: What options do we have?
Source: IEA 2014:Technology Roadmap for Energy storage

## Slide 10
Electricity
Hydrogen
CH3OH
HCOOH
NH3
H2 storage
Fuel cells
Electrolyzers
Fuel cells
Catalysis
Batteries
Motivation: Materials for energy conversion and storage

## Slide 11
11
Hydrides: Multifunctional materials

## Slide 12: (Complex) metal hydrides: Multifunctional energy materials
12
Catalysis
Luminescence
Sensing
Nuclear shield
Ngene, P. Dam, B. et al., Adv. Funct. Mater. 2014, 24, 2374. Nature Communications 2017, 8, 1846
Qianru Wang, et al. Joule, Volume 4, Issue 4, 2020, 705-709,
H2 sensing/detection
Hongen Yu et al. ACS Catalysis 2024, 14, DOI: 10.1021/acscatal.3c05696
Catalysis
Properties-Functionality relationship

## Slide 13
Züttel et al., Phil. Trans. R. Soc. 2010 vol. 368
Hydrogen
High Energy density
Why hydrogen
H2 is most promising for long-term carbon-free seasonal storage
From EC 2050 Scenario analysis by McKinsey

## Slide 14
Key figures:
35 kg of H2 350 bar regenerative breaking
>250 km range
Why hydrogen storage?

## Slide 15: H2 storage: why is it a big challenge ?
 | per kg [kWh/kg] | per liter [kWh/l]
Gasoline (liquid) | 12 | 8.6
Hydrogen (gas) | 33 | 0.003
Ambient conditions:
40 liter gasoline
34 x 34 x 34 cm
58,182 liter H2 (5 kg)
3.9 x 3.9 x 3.9 meter
High gravimetric but low volumetric energy density
tank

## Slide 16
High pressure cylinders
Liquid hydrogen storage (-253 °C)
Molecular adsorption on high surface area materials (OMMs)
Solid hydrogen storage in metals and alloys, complexes ( mgH2, LiH)
Hydrogen storage methods
Ambient conditions:
40 liter gasoline
34 x 34 x 34 cm
58,182 liter H2 (5 kg)
3.9 x 3.9 x 3.9 meter
45 kg LiBH4
27 x 27 x 27 cm
LiBH4 LiH + B +1.5 H2
ΔT, Δ P

## Slide 17: Hydrogen storage in metals (metal hydrides)
high storage capacity (weight, volume)
cost, mechanical properties
cycling stability
release by a trigger at relevant conditions
  Pressure
  Temperature
  UV light
  …

## Slide 18
DOE Target: >5.5 wt% H2 at 100-150 °C
LiBH4
Poor H2 release kinetics
Poor reversibility (350 bar H2, 650 °C for LiBH4)
Reversible H2 storage in metal hydrides
Equilibrium decomposition
(1 bar H2 equilibrium)

## Slide 19
Metal hydride
Nanoscaffold
(carbon, MOFs, SiO2)
Why Nanoconfinement?
particle size effects
Hydride-support interaction
Restrict phase segregation
Approach: Interface engineering by nanoconfinement
Clamping/physical constraint
2LiBH4 2LiH + 2B + 3H2

## Slide 20
P.L. Bramwell, P. Ngene, P.E. de Jongh. Int. J. Hydrog. Energy 42 (2017) 5188
P. Ngene, A. P.M. Kentgens and P. E. de Jongh. et al Nano Energy 22, (2016)169
Ngene, de Jongh, et al. Energy Environ Sci. 2012, 4, 4108,
Chem. Commun. 2010, 46, 8201, Faraday Disc, 2011, 151,
(7.9 wt% H2)
(8.1 wt% H2)
Reversible H2 storage in nanoconfined metal hydrides
(13 wt% H2)
(18 wt% H2)
Reversibility (H uptake after decomposition)
What is the origin of the improved kinetics
Hydride-support interaction?
Change in decomposition pathway?

## Slide 21
Probing Nanocomposites with Xray Raman Scattering (XRS)
Absorption of a photon with energy equal to the binding energy of the core electron (element specific)
For low absorption edges (Li, C, B, Na, F, N, Mg) soft XAS is used
Soft XAS: requires complicated experimental conditions
Thin samples required
High vacuum (all components)
Not in-situ
Concentrated samples due to low sensitivity
Mostly surface information (< 50 Å)
hole
X-ray absorption

## Slide 22
Interface composition: Xray Raman scattering (XRS)
Superb for light elements, overcomes experimental challenges of Soft XAS
Similar to Raman scattering in optics
Core electron excited to continuum while a photon changes its energy from Ei to Ea
If ΔE (Ei-Ea)= BE → sample info.
Scattering probability is angular dependent
U. Bergmann et al. Microchemical Journal 71 (2002) 221–230
S. Huotari, Ch. J. Sahle et al. J. Synchrotron Rad. (2017). 24, 521–530
Absorption of a photon with energy equal to the binding energy of the core electron
Analyzer (fixed energy)
ΔE (Ei-Ea)= BE
→ sample info
10,540-10000= 540 eV
Notes: The process is in principle analogous to X-ray absorption (XAS), but the energy transfer plays the role of the X-ray photon energy absorbed in X-ray

## Slide 23
17
11
Output
X-ray beam(E0)
Scattered X-rays (Ef)
Measurement cell
Raw data
Intensity maps from 12 or 60 detectors
Kapton
Sample
Compton scan
Normalized spectra
Addition of ROIs of one scan
Addition multiple scans and background substraction
B-edge
Na-edge
B-edge
Based on Sahle, C. J., et al. J. synchrotron radiation 22.2 (2015): 400-409.
XRS measurements overview (SSRL, DESY, SOLEIL and ESRF)

## Slide 24
SSRL beamline BL6-2 ES2
Analyzer energy: 6.5 keV
Resolution of 0.3 eV.
XRS on LiBH4/C nanocomposites
Investigate the evolution of phases upon heating.
Bulk LiBH4 shows different behaviour from nanoconfined
Miedema, Ngene, de Jongh, de Groot, et al. PCCP, 2012, 14, 5581–87, PCCP 2014, 16, 22651-58

## Slide 25
Miedema, Ngene, de Jongh, de Groot, et al. PCCP, 2012, 14, 5581–87, PCCP 2014, 16, 22651-58
XRS on LiBH4/C nanocomposites
C K-edge
B K-edge
Li K-edge
B-O bond?
Sample partially reversible so not completely B-O (LiBO2)

## Slide 26
LiBH4 + 6 C ↔ LiC6 + B + 2H2 (18 wt.% H)
LiBH4 ↔ LiH + B + 1.5 H2 (13.5 wt.% H)
Li intercalation into the graphene layers stabilizes Li, destabilizes nanoconfined LiH
Ngene, de Jongh, et al. Nano Energy, 2016, 22, 169
XRS on LiBH4/C nanocomposites: Li intercalation?

## Slide 27
Nature( 2015), 526, S93
Solid electrolytes and rechargeable batteries
Notes: In past decades rechargeable battery have emerged as high specific power portable energy storage devices
Extensively used in mobile phones, upcoming in electric vehicles and possibly utilized for large-scale on-site grid energy storage

## Slide 28
13MW Lakeland Solar & Storage Project in Queensland Australia
Powers 4,015 average home air-conditioning units simultaneously for eight hours through the day
Large scale electricity storage with batteries
Project cost $17.4M (mostly due to batteries)

## Slide 29
Conventional car: combustion engine 8 liters per 100 km
Electric vehicle:
20 kWh per 100 km
Electric cars are way more efficient compared to electric engines. Factor 3-4 !!
Batteries can transform chemical to electrical energy (and vice versa) with extremely high efficiency because the entropy change is very small
Transitioning to electric vehicles is a huge opportunity to save energy!
8 liters of gasoline (heating value) = 70 kWh per 100 km
Energy use by sector
Battery and sustainability

## Slide 30: Increasing energy density, decreasing cost
Shirley Meng et al. Nature Energy 2022
Plackeet al., J. Solid State Electrochem. 2017, 21, 1939

## Slide 31: Next-generation batteries

## Slide 32: Limitations for Li-ion batteries
Anode
LiC6
Cathode
LiCoO2
Eelectrolyte
LiPF6, LiCFSO3 in
high-boiling sol
vent (carbonates, ethers)
Safety issues
(evaporation and decomposition of electrolyte)
P.C. Howlett et al. , J. Pow. Sources, 114(2003), 277-284
Limited Energy density
(new battery chemistry ASSB)
High price of Li
(Na, Mg , other battery chemistries

## Slide 33: From liquid to solid electrolytes for batteries
Anode
LiC6
Cathode
LiCoO2
Electrolyte
Improved safety: (prevent dendrites, high chemical and thermal stability)
Higher capacity electrodes (Li metal, sulfur: Li-S), 5-10 times increase in energy density
Inexpensive batteries: (Na, Mg, Cl- F- batteries)
Anode
Li
Cathode ( S)
Solid electrolyte

## Slide 34: Fast Li- and Na-ion conduction in complex hydrides
34
High ionic conductivity but only at high T (LiBH4 > 110 oC)
Can the high-temperature phase be stabilized?
Orthorhombic
~10-8 S cm-1
at 30 oC
Hexagonal
~10-3 S cm-1
at 120 oC
Matsuo & Orimo, Adv. En. Mater. 1 (2011) 161-172., Appl. Phys. Lett. 91 (2007), 224103
n: concentration of ions q: ion charge
μ:mobility of ion carrier Ea: activation energy

## Slide 35
Approach: Interface engineering-Nanocomposite electrolytes
D. Blanchard, P.E. de Jongh et al., Advanced Functional Materials 25.2 (2015): 184-192.
L. M. de Kort, V. Gulino, P. E. de Jongh, and P. Ngene, Journal of Alloys and Compounds 901 (2022): 163474.
SBA-15 SiO2
6 nm pores
Ngene, de Jongh et al, JPCC,114, (2010), 6167

## Slide 36
LiBH4/SiO2
bulk LiBH4
ASSB-based on LiBH4/SiO2 nanocomposite
Blanchard, Ngene, de Jongh, et al., Adv. Funct. Mater. (2015), 25, 184, ACS appl energy materials 2023,

## Slide 37
50 nm
25 v/v %
9
Effect of different metal oxides
V. Gulino, et al., ACS Applied Energy Materials 3.5 (2020): 4941-4948.

## Slide 38
50 nm
9
Effect of different metal oxides, and hydrides
Gulino, Ngene, de Jongh, et al., ACS Applied Energy Materials 3.5 (2020): 4941-4948.
About 1000 x increase in conductivity upon nanoconfinement
Applicable to Li, Na, and ion-substituted hydrides (LiBH4-LiNH2,)
The nature of the oxide influences ionic conductivity
A complex interplay between the properties of hydride and the oxide insulator
R. Zettl, L.M. de Kort, Ngene P. et al. Journal of Physical Chemistry C 124.5 (2020): 2806-2816.
L.M. de Kort, de Jongh P., Ngene P., et al. Journal of Materials Chemistry A 8.39 (2020): 20687-20697
L.M. de Kort, Ngene P., et al. Advanced Functional Materials 33 (2023) 2209122

## Slide 39
ID20 @ ESRF Grenoble
ID20 ESRF
Analyzer energy: 9690 eV
Resolution of 0.7 eV
Detector: Medipix (72: 12 X 6)
Imaging capability
2θ = 50–60°
2θ = 55° (DESY)
XRS on LiBH4/oxide nanocomposites
Notes: At ESRF, the XRS spectra were collected using Medipix detectors (2D photon-counting X-ray detectors with a 55 µm spatial resolution) with an average q-vector of 4.1 to 4.9 Å−1 (2θ = 50–60°). At DESY, the XRS spectra were collected using Medipix detectors with an average q-vector of 4.5 Å−1 (2θ = 55°).

## Slide 40
Presence of B-O bonds in the nanocomposites
Not completely oxidic B because LiBO2, is not conductive
Si-O-BHxLi? Interface composition depends strongly on the oxide used
XRS: LiBH4/SiO2 nanocomposites

## Slide 41
XRS: LiBH4/oxide nanocomposites
Conductivity is proportional to the amount of the trigonal B !
L. M. de Kort, M. Lazemi, A. Longo, V. Gulino, H. P. Rodenburg, D. Blanchard, C. Sahle, M. Sundermann, H. Gretarsson, A. M. J. van der Eerden, H. Elnaggar, F. M. F. de Groot, P. Ngene, Adv. Energy Mater. 2024, 2303381
V. Gulino, A. Longo, L. M. de Kort, H. P. Rodenburg, F. Murgia, M. Brighi, R. Černý, C. J. Sahle, M. Sundermann, H. Gretarsson, F. de Groot, P. Ngene, Small Methods 2024, 8, 2300833.

## Slide 42
XRS: What have we learned?
Surface or interface interaction is crucial

## Slide 43
Influence of oxide surface chemistry?
Drying changes the silanol density and influences ion conductivity.
Surface interaction matters!!
Methyl-modified (functionalized) SBA-15 exhibits the lowest ionic conductivity!
P. Ngene, S. Lambregts, P.E de Jongh et al. PCCP 2019, 21, 22456 - 22466
SBA-15 (6nm, 800m2/g)
SBA-15 (10nm)
~600m2/g)

## Slide 44: Conclusions
(Complex) metal hydride nanocomposites are a promising class of energy materials: reversible hydrogen storage, solid electrolytes for batteries (also hydride ion conductors)
Interface effects play a crucial role in their properties
Synchrotron-based x-ray (and neutron) techniques are crucial to materials discovery
..there is still a lot to understand…!

## Slide 45
Acknowledgement

## Slide 46
Thank you
Acknowledgement
ID 20:
Christoph Sahle, Alessandro. Longo
PO1
Martin Sundermann, Hlynur Gretarsson