## Slide 1
Debye Institute for
Nanomaterials Science
21st September 2022
X-ray absorption spectroscopy & Resonant inelastic x-ray scattering
Frank de Groot
l.barberis@uu.nl
NWO CHAINS 2022
f.m.f.degroot@uu.nl

## Slide 2
X-ray absorption spectroscopy (XAS)
Resonant inelastic x-ray scattering (RIXS)
Virtual beamlines
XAS & RIXS

## Slide 3
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS of transition metal oxides
Electronic structure of a transition metal oxide
Main bonding:
O2p with metal 4sp
Gives valence band and conduction band,
Mixed in character
Additional bonding
O2p with metal 3d;
Gives mixed 3d bands split by crystal field in octahedral symmetry, T2g states have pi-bonding and Eg states have sigma-bonding.
oxygen 1s core state
is localized at an oxygen atom
Notes: 3

## Slide 4
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
transition from oxygen 1s state
to an empty state
oxygen 1s core state
is localized at an oxygen atom
local empty DOS
dipole selection rule:
p-projected DOS
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
[Phys. Rev. B. 40, 5715 (1989); review in Chem. Rev. 120, 4056 (2020)]
XAS of transition metal oxides
Notes: 4

## Slide 5
oxygen 1s XAS
Crystal structure
Electronic structure calculation, for example Density Functional Theory (DFT)
(in the presence of the core hole;
or TDDFT/BSE)
Calculation of the oxygen
p-projected local empty DOS
Compare with experiment
CODES: FEFF, Wien2K, VASP, QE, etc.

## Slide 6
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
Expect local empty DOS
Expect the d (and s-) projected DOS
Why is experiment different?
Metal 2p XAS
Notes: 6

## Slide 7
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
Expect local d-projected DOS
Core spin-orbit splitting
Metal 2p XAS
Notes: 7

## Slide 8
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
Expect local d-projected DOS
Core spin-orbit splitting
Overlap of core 2p and valence 3d states
Metal 2p XAS
Notes: 8

## Slide 9
Can NOT neglect 3d-3d interactions
Can NOT approximate 2p-3d interaction as extra potential
Large core hole spin-orbit coupling
IXAS = |< 2p5 3d6 |dipole| 3d5>|2 [E=0]
CODES: CRISPY/QUANTY, CTM4XAS
[Phys. Rev. B. 42, 5459 (1990); REVIEW: J. Elec. Spec 249, 147061 (2021)]
Metal 2p XAS

## Slide 10
calculate energy states (DOS)
dipole transition to empty DOS
apply multiplet theory
structure of molecule or solid
1s ↔ 2p
XAS spectral shape
(ask via email)

## Slide 11
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: Combination with x-ray microscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RPES, R diffraction
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 12
X-ray absorption spectroscopy (XAS)
Resonant inelastic x-ray scattering (RIXS)
Virtual beamlines
XAS & RIXS

## Slide 13
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV

## Slide 14
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
IR
UV/Vis

## Slide 15
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
(Resonant) Raman

## Slide 16
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
Resonant X-ray Raman
= RIXS
Resonant Inelastic
X-ray Scattering

## Slide 17
Resonant Inelastic X-ray Scattering
I20 at Diamond, UK

## Slide 18
Resonant Inelastic X-ray Scattering
Energy
Polarization
Momentum
Eout ,kout, eout
Ein, kin, ein
q = kin - kout
h𝝎= Ein - Eout
Eout, ,kout, eout
Ein,, kin, ein

## Slide 19
RIXS (resonances)
Transfer of:
Energy
Momentum
Polarization
Notes: 19

## Slide 20
Ψ0
3 2 1 0
2p3d RIXS of transition metal ions
core
electronic
dd, CT
magnon
vibrations

## Slide 21
Δω-RIXS: energy dependence
Δk-RIXS: momentum dependence
Δε-RIXS: polarization dependence
Resonant Inelastic X-ray scattering
Δω-RIXS of Fe2O3 Δk-RIXS of LaCoO3 Δε-RIXS of Fe3O4
Nat.Comm. 14,2749 (2023) PRB 98, 035149 (2018) ACS Appl.Mat.11, 36213 (2019)

## Slide 22
Momentum dependent dd excitations (LaCoO3)
q-dep. RIXS
[Wang et al. Phys. Rev. B. 98, 035149 (2018)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 23
dd
spin-flip
‘spin-flip’
MS
S
2p3d RIXS of NiO
[Phys. Rev. B. 57, 14584 (1998)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 24
2p3d RIXS of NiO
[Nag, Phys. Rev. Lett. 124, 067202 (2020)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 25
2p3d RIXS of Fe2O3
[Elnaggar, Nature Comm. 14, 2749 (2023)]

## Slide 26
2 photons
=
2 spin flips
Ground State:
3d5
Sz = 5/2
Fe3+ Ion
Elastic
ΔMS = 0
Classical Magnon
ΔMS = 1
Double Magnon
ΔMS = 2
2p3d RIXS of Fe3+ ions (atomic)

## Slide 27
Ground State:
3d5
Sz = 5/2
Fe3+ Ion
ΔMS=3,
E ~ 0.3 eV
ΔMS=4,
E ~ 0.4 eV
ΔMS=5,
E ~ 0.5 eV
2p3d RIXS of Fe3+ ions (octahedral)
Elnaggar et al, Nature Communications 14,2749 (2023)

## Slide 28
Element specific
Applicable under extreme conditions (hard x-rays)
Momentum dependent phonons, magnons
Remove lifetime broadening
High-resolution & operando (hard x-rays)
Valence-selective EXAFS (hard x-rays)
Resonant Inelastic X-ray Scattering
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 29
X-ray absorption spectroscopy (XAS)
Resonant inelastic x-ray scattering (RIXS)
Virtual beamlines
XAS & RIXS

## Slide 30
Virtual beamlines (XAS, RIXS, EXAFS, XMCD)
Develop theoretical spectroscopy students/groups
Develop knowledge of synchrotron user communities
Assist in beamline proposals at existing synchrotrons
Virtual synchrotron

## Slide 31
Virtual beamline: Only need group of smart students
Can be developed at every university/institute
I would be pleased to help/assist f.m.f.degroot@uu.nl
Virtual synchrotron