## Slide 1
Evaluating the Impact of Substrate Thickness on the Structural Integrity of Plasma-Sprayed Hydroxyapatite Coatings
Tshepo Ntsoane
Necsa Research and Innovation
22 November 2024

## Slide 2
Introduction
Sample preparation
Experimental
Results and discussion
Conclusion
SA’s ESRF membership
Outline

## Slide 3
Introduction
Worldwide, an increasing number of patients rely on biomedical implants for repair and replacement of body parts to restore lost functions such as mobility. Applications of biomaterial ranges from hip implants to intraocular lenses for eye surgery. Factors contributing to this include:
Aging population,
Longer life expectancies,
Embrittlement due to osteoporosis in elderly patients mostly women,
Increasing number of accident incidents in young people.

## Slide 4
Introduction cont.’
Global orthopedics market share - ~US$40.5B (2018) with a growth of 4.4% compared to the previous year. The projected growth is expected to reach US$67.9B by the end of 2023 with growth rate of 3.3%.

## Slide 5
Introduction cont.’
Biomaterials: Metals, Ceramics, composites
Choice depends on the application.
Load bearing application, hydroxyapatite (Ca10(PO4)6((OH)2, owing to it’s similarity to the mineral component of the bone
Disadvantage: Poor mechanical properties
  Brittleness: Limitation in load bearing application
  Coated on a metallic substrate such as Ta, Steel etc.
Coating techniques:
  Sol-gel, Sputter coating, PLD, Electrophoretic deposition, Dip coating
  Thermal spraying

## Slide 6
Thermal spray
Introduction cont.’
Aim: Investigate the effect of substrate thickness on thermal spray coating. Phase identification, crystallinity and residual stress
Although excellent coating results have been observed, studies have shown coating do failure (adhesively and cohesive)

## Slide 7
Sample Preparation
https://www.sciencelearn.org.nz/images/250-plasma-spray-process

## Slide 8
Sample preparation cont.’
Parameter | Value
Primary plasma gas (Ar) | 45 slpm
Secondary plasma gas (H2) | 6.5 slpm
Carrier gas (Ar) | 5 slpm
Relative powder feed rate | 20 %
Relative hopper stirrer rate | 40 %
Spray distance | 90 mm
Plasma power | 30 kW
Horizontal speed | 0.1 m/s
Traverse speed | 0.017 m/s
Spraying parameters
SBF salts
Ionic concentration comparison

## Slide 9
Near-surface investigation
Experimental
Strain scanner

## Slide 10
Near surface region
Results

## Slide 11
Near surface : PIXE
Results cont.’

## Slide 12
Results cont.’

## Slide 13
Results cont.’

## Slide 14
Near surface residual stress
Results and discussion

## Slide 15
Results and discussion cont’

## Slide 16
Origin of residual stresses (RS)

## Slide 17
Depth resolved investigations
Experimental

## Slide 19
Depth resolved investigation
Results cont.’

## Slide 20
Depth resolved phase composition
Results

## Slide 21
Disk
Depth resolved phase composition

## Slide 22
Cylinder
Depth resolved phase composition cont.’

## Slide 23
Disk : Normal planar stress
Depth resolved residual stress

## Slide 24
Shear components

## Slide 25
Cylinder

## Slide 26
Shear component

## Slide 28
In both geometry, HAp is the predominant phase with TTCP the main thermal product across coating thickness.
HAp and thermal products increases initially and decreases respectively with immersion before subsequently decreasing and increasing gradually
The high and low crystallinity indices at the near-surface and near-interface region of the coating respectively predominantly amorphous near-interface region respectively.
Microscopy studies revealed a secondary HAp precipitate forming on the coating surface after 28 days of immersion; the precipitate grows in thickness and surface area with immersion period. Cross-section analysis indicated that the precipitate extends deeper into the coating through a network of channels.
Residual stress concentrated in the near-surface region
Higher residual stress observed in the cylinder.
Conclusions

## Slide 29
SA’s ESRF membership
  Medium Term Agreement
  Initial signed 2013, renewed number of times. Current agreement 2025
  Non-proprietary use of the facility
  Level @ 0.3%
  Access to beam time
    Travel costs, Accommodation, Meals (Canteen card)
  Training of Post-Docs, scientists
Government support: Access and mobility

## Slide 30
Dr T.T. Thabethe (UP)
Prof J.B. Malherbe (UP)
Prof C. Theron (UP)
Ms Unaisa Dockrat (UP)
Necsa Applied Radiation
Dr Jon Almer (APS)
Dr Rob Robinson (APS)
Acknowledgements