## Slide 1: Thermal expansion behaviour of BPO4 studied by X-ray thermodiffractometry
Wilson Mogodi
Notes: Two themes of this presentation
Going to inspire you why pxrd is exciting and why you should use it… eng, phy, material scince, chemistry viz. how powderful PXRD can be
Broad overview of the research in my PhD.

## Slide 2: Borophosphates
Borophosphates = Intermediate compounds of the systems
MxOy­­-B2O3-P2O5-(H2O)
(M = main group/transition metal, ammonium)
Are a young class of materials.
Exhibit large variety of connection pattern of the anionic unit ∞[BxPyOz]n-.
From this, diverse and exciting materials have been synthesized:
Traditional functional materials; aluminosilicates and metal phosphates have been extensively used.
Notes: Ion exchange, separation and catalysis.
Borophoshates; have some structural similarity of aluminosilicates and metal phosphates

## Slide 3: Borophosphates: Three-dimensional open framework/porous
Yang et al. Dalton Trans., 2011, 40, 2549
Technological importance in shape-selective catalysis and ion exchange applications.
Examples:

## Slide 4: Borophosphates: Low-porosity anhydrous phases
Kniep et. al. Chem. Mater. 1998, 10, 2930 - 2934
Borophosphate anion includes isolated species, oligomers, chains and even layers.
Notes: Isolated = Isolated trigonal planar borate and tetrahedral phosphate (red polyhedra) species
Double single = Isolated trigonal planar borate sharing an oxygen with phosphate tetrahedron and two isolated phophate groups

## Slide 5: Non-porous Borophosphate
Thermal expansion behaviour of BPO4
Thermal Expansion:
Low Positive Thermal Expansion (LPTE) = Minor Expansion when heated
Zero Thermal Expansion (ZTE) = No Expansion/Contraction when heated
Negative Thermal Expansion (NTE) = Contract when heated

## Slide 6: BPO4: Structure-property relation
BPO4 of interest because of its isostructural relationship with SiO2.
Two polymorphs:
High-cristobalite-type Quartz-type
Tetragonal lattice, space group I4
Trigonal lattice, space group P3121
Notes: BPO4: Structure-property relation = How the crystal structures provide an explanation for the unusual thermal expansion behaviour.
In both structures, the crystal structures are build of corner sharing BO4 and PO4 TETRAHEDRAL UNITS.
Quartz = Under high temperature and pressure conditions.

## Slide 8: ESRF ID22 Powder Diffractometer
Nine channel multianalyser stage
Notes: Nine channel multianalyser stage

## Slide 9: 2D flat panel detector for fast PDF
41 x 41 cm2 Perkin Elmer XRD 1611 medical imaging detector

## Slide 10: Variable temperature PXRD results for BPO4
Collection of 19 diffractograms. Each diffractogram was analysed via Rietveld refinement method.
30 °C
900 °C
2θ
Notes: Stack plot of diffraction patterns one on top of the other.

## Slide 11
Highly anisotropic lattice (c/a value is 1.52 at 30 °C).
In temperature range 30-900 °C :
αa/b = 10.5 ppm/°C
αc = 2.71 ppm/°C
αv = 24.0 ppm/°C
By definition, BPO4 is a low positive thermal expansion material.
Unit cell dimensions as a function of temperature

## Slide 12: Interpolyhedral distances and Atomic displacement parameters
Bond length (Å)
B (Å2)
Unphysical decrease in P-O bond and increase in B-O bond lengths with temperature.
The increase in thermal motion of O atoms lead to shortening of P-O bond. Also seen in Y2(WO4)3, Sc2(WO4)3 (Evans and co-workers)
B
O
P

## Slide 13: Dynamic disorder in BPO4
The oxygen atom between tetrahedral can rotate about the bond axis
In conventional (Bragg) diffraction analysis:
Average positions of the atoms = the centre of the distribution of positions
Amplitude of thermal motion = the width of the distribution of the positions
Bragg diffraction does not measure bond lengths directly:
Associate average positions of two atoms with interatomic distances (bond lengths)
The mid point of the distribution determined by the analysis may not be the true midpoint
Tucker et al. 2000
Notes: Reason for average structural model failing at low r:

## Slide 14: Dynamic disorder in BPO4
Consequently from Bragg analysis:
The P-O-P bond in the average structure is straight
True P-O-P bond should be around 130 and oxygen atom rotates around bond
Tucker et al. 2000
Notes: Reason for average structural model failing at low r:

## Slide 15: Pair distribution function, G(r)
Total Scattering = Bragg + Diffuse Scattering
G(r) =
S(Q) is the powder diffraction pattern that has been corrected for experimental artifacts and normalised
The PDF is a measure of the probability of finding pairs of atoms in the material separated by a distance, r.
Peaks in the PDF correspond to the actual bond lengths
Notes: Reason for average structural model failing at low r:

## Slide 16: G(r) function of BPO4 at 30C
r(Å)
G(r)
Rw = 25.64 %
The first peak in the G(r) corresponds to the B-O and P-O bonds
P - O
B - O
Notes: stereochemical restraint refinement
The weighting factors, tol, defines the weighting given to the particular stereochemical restraint.
Applies penalties restraining distances and angles between sites

## Slide 17: Variable temperature PDF experiment of BPO4
30 °C
900 °C
The B-O and P-O bond lengths was extracted from all measurements

## Slide 18: Interpolyhedral distances
Bond length (Å)
Bragg analysis
Bond length (Å)
PDF analysis
Notes: Modest increase in P-O distance as a function of temperature

## Slide 19: Interpolyhedral angles and distances
Increase in B-O-P bond angle (θ) with temperature.
This increase in bond angle is reflected by an increase in B--P separations.
Contributes to an increase in the a and c lattice parameters.
B
O
P
θ

## Slide 20: Conclusions
The variation in the crystal structure provides an explanation for this low thermal expansion behaviour.
Common feature of thermally stable/robust materials:
    Strong covalence of chemical bonds i.e. B-O and P-O.
    Flexible crystal structures.
Future work: “Big”-box refinements
(vs “Small”-box refinements)
Notes: A relationship between the synthetic approach and the resulting crystal structure of the borophosphate compounds was also established.
Strong covalence of chemical bonds i.e. B-O and P-O = lead to rigid polyhedra

## Slide 21
Bond length distribution

## Slide 22: Bond angle distribution

## Slide 23: Acknowledgements
University of the Witwatersrand
David Billing
Manuel Fernandes
Andy Fitch
Catherine Dejoie
Carlotta Giacobbe
Mauro Coduri
Olivier Grimaldi