## Slide 1: Pb-doped Bismuth Oxide Electrolyte Materials for Intermediate Temperature Solid Oxide Fuel Cells
Emileo Naicker
PhD student
Supervised by
Prof C. Billing and Prof DG. Billing

## Slide 2: Outline
Importance of this research
Electrolyte and Dopants
Conductivity performance
Powder X-ray diffraction from Synchrotron (SSRL)

## Slide 3
Clean energy – environmentally friendly
CO2 production resulting in global warming – climate change

## Slide 4: Electrolyte
help with conductivity
help with stability of the fcc phase
help with aging
Dopants
Bismuth oxide as an electrolyte due to its extremely high conductivity in the face centered cubic (fcc) phase
Pure bismuth oxide is only stable in the fcc structure between 730-824oC which is not optimal for the cell operation and longevity
Aim
This work aims to use a combination of yttrium and cerium to stabilise the fcc phase and lead to increase conductivity.
Pb
Y
Ce

## Slide 5
Bismuth Oxide pellet synthesis and EIS measurement
Synthesis
Citrate gel method
Mix correct stochiometric amounts to produce
20Y10Ce10Pb and 20Y10Ce5Pb systems
Bruker D2 Phaser instrument was used for initial phase identification
Measurement
uniaxial cold press at a constant pressure of 500 MPa with Poly Vinyl Alcohol
Electrochemical impedance spectroscopy (EIS) was done using the MTZ-35 frequency with a 10mV amplitude
EIS was done between 350 °C to 750 °C
Bismuth Oxide pellet

## Slide 6: Arrhenius Plot and Conductivities
Temperature (o C) | 20Y10Ce10Pb (S.cm-1) | 20Y10Ce5Pb (S.cm-1)
350 | 2.58E-06 | 2.28E-06
450 | 0.0001 | 7.97E-05
550 | 0.002558 | 0.002041
650 | 0.022568 | 0.018158
750 | 0.096008 | 0.07583

## Slide 7
Stanford Synchrotron Radiation Lightsource

## Slide 8
2 theta(degrees) λ= 0.7288 Å
DIFFRAC.TOPAS software use for Rietveld Refinement using Bismuth yttrium oxide cubic (Fm-3m) structure
Room Temperature Measurement

## Slide 9
2 theta(degrees) λ= 0.7288 Å
Variable Temperature measurement between 350oC to 600oC

## Slide 10
2 theta(degrees) λ= 0.7288 Å
750oC Measurement

## Slide 11
775oC Measurement
2 theta(degrees) λ= 0.7288 Å

## Slide 12
Pellet after measurement
Before
After

## Slide 13: Conclusions and Future work
Pb works within a certain temperature range
At 750oC lead starts to migrates from structure
Raman Spectroscopy on Pellets
Longer conductivity measurements at certain temperatures

## Slide 14: Acknowledgements

## Slide 15: Questions
1833066@students.wits.ac.za