## Slide 1
Prof. R. BAGTACHE
Laboratory of Electrochemistry-Corrosion, Metallurgy and Inorganic Chemistry, Faculty of Chemistry,
(USTHB), BP 32, 16111, Algiers, Algeria
LABORATOIRE ELECTROCHIMIE CORROSION METALLURGIE CHIMIE MINERALE
LECMCM

## Slide 2: Synthesis and Characterization of Aluminophosphate. Application to photodegradation of Methyl Violet Dye

## Slide 3: Outline
Introduction
Synthesis
Application
Results and discussion
Conclusion

## Slide 4
Introduction

## Slide 5
Porous material possess internal voids or pores, allowing for internal distributions that can be tailored to improve overall performance, such as mechanical, thermal, and acoustic properties. These properties are enhanced through designs like functionally graded porosity, which involves varying pore size and density along one or more directions.
Introduction

## Slide 6
Porous materials offer great potential due to their properties such as high specific surface area, low density, and high specific strength. Their structure, characterized by continuous and interconnected porosity, facilitates the transport of electrons, ions, and particles.
The chemical compositions of porous materials are well-controlled and diversified and include metals, ceramics, and carbon-based materials. As a result, the development of porous materials is quickly gaining significance. An increasing number of researchers are working to conduct fundamental research on various applications from different perspectives
Introduction

## Slide 7
Introduction

## Slide 8
Introduction
Porous
materials

## Slide 9
At the onset of 1980’s, the Union Carbide laboratories reported a new family of molecular sieves based on aluminophosphates (AlPO-n).
The aluminophosphates (AlPO-n) are microporous inorganic solids with structural and chemical properties similar to those of zeolites, which are naturally occurring and synthetic aluminosilicates.
They are composed of Al and P atoms arranged in a neutral structure. Their crystalline framework, which is built from alternating AlO₄ and PO₄ tetrahedral units and their general formula can be expressed as [(AlO2)x·(PO2)x]·yH2O. These structures can be similar or different to zeolites.
Introduction

## Slide 10
In this context, we report the synthesis and its physical characterization of potassium aluminium fluoride phosphate KAlPO4F, that was further applied in the removal of Methyl Violet.
Introduction

## Slide 11
Adsorption and Gas Separation
Catalysis
Ex: with Ti can act as catalysts
Thermal Energy Storage
Some microporous AlPOs are used for water-based thermochemical energy storage (sorption heat storage) — they adsorb and desorb water
Applications of AlPO-n
Their micropores, AlPOs can selectively adsorb gases. Narrow-pore AlPOs (8-ring) are studied for CO₂ separation
Mechanical/ Structural Uses
Their unusual mechanical behavior (like negative linear compressibility) might be exploited in materials science

## Slide 12
Characterization
Distilled water
Phosphoric Acid
Aluminium Source
A remineralizing agent
Crystallization
Filtration
Washing and Drying
SYNTHESIS PROCEDURE
Hydrothermal route
at 180 °C, 3 days
AlKPO4F

## Slide 13
XRD pattern
SEM image
Thermal analysis
UV-vis refelectance diffuse
Characterization

## Slide 14
Application

## Slide 15: Photocatalysis
Photocatalysis is a physicochemical process that requires two components :
A catalyst and light
Its principle consists of the action of a catalyst, which must be a semiconductor activated by a natural or artificial light source.
Application

## Slide 16
Application of photocatalysis
  Insecticides
  Pesticides
  Dyes
Degradation of various pollutants
  Bacteria
  Fungi
  Viruses
Destruction of
Micro-organisms
  Elimination of atmospheric nitrogen oxides
  Odor elimination
  Self-cleaning surface coatings
Air purification
  Hydrogen or oxygen production
  Synthesis of organic compounds
  Cancer treatment
Others
Application

## Slide 17
Page 15
Advantages of photocatalysis
Operates at room temperature
Possibility of total mineralization: formation of H2O and CO2
Low energy consumption
Effective at low pollutant concentrations
Catalysts in various physical forms
Application

## Slide 18
Application

## Slide 19
Application

## Slide 20
Application

## Slide 21
Application
λmax (= 582 nm)
Chemical formula of Methyl Violet (MV): C25H30ClN3

## Slide 22
Results and discussion

## Slide 23
XRD pattern prepared by hydrothermal route.
Space Group: Pnna, with the lattice constants:
a=12.612(5) Å, b=10.172(3) Å, c=6.205(0) Å

## Slide 24
Projection of the crystal structure along [001] axis

## Slide 25
SEM image

## Slide 26
Chart: Temperature (°C)
Thermal analysis

## Slide 27
UV–Visible diffuse reflectance
(h)m = constant  (h - Eg)
Where h (eV) is the incident photon energy and  (cm-1) the optical absorption coefficient

## Slide 28
Results : application
RD % = [(C0-Ct) / C0] *100
RD%: percentage of degradation
C0 : the initial concentration of the dye
Ct : the concentration at time t
The remaining MV concentration was evaluated by measuring the absorbance at λmax (= 582 nm). The adsorbed amount was calculated from the following expressions:

## Slide 29
Application
Changes in the absorption spectrum of MV under sunlight

## Slide 30
The aim of this work is the search for crystalline materials, of the aluminophosphate type.
The phase was isolated in crystal form. The oxofluorophosphate KAlPO4F, a novel photocatalyst, was prepared by hydrothermal route at 180 °C.
Through this study, we have tried to get as close as possible to the structural framework by characterizing it using several other techniques, primarily:
X-ray powder diffraction
SEM/EDX
Thermal analysis
UV-visible diffuse reflectance spectroscopy
Conclusion

## Slide 31
Conclusion
The X-ray diffraction, revealed an orthorhombic system with the lattice constants: a=12.612(5) Å, b=10.172(3) Å, c=6.205(0) Å.
The structure is made up of AlF2O4 octahedra and PO4 tetrahedra where the K+ ions are
disordered.
SEM images shows crystals with hexagonal sections.
Thermal analysis shows that our phosphate is thermally stable up to 300 °C.
The direct optical transition of 4.93 eV, determined from the diffuse reflectance, is assigned to the charge transfer F− : 2p → K+ : 4 s.
The photocatalytic performance was successfully tested through the degradation under solar light of methyl violet (MV), a hazardous and persistent dye. A total discoloration was obtained after 5 h

## Slide 32
Thank you for your attention