## Slide 1
RUTHERFORD BACKSCATTERING ANALYSIS USING LITHIUM IONS
Trevor Derry, Morgan Madhuku and Tony Miller.
WITS, iThemba LABS (G) & the DST-NRF CoE-SM

## Slide 4: Lithium-7 RBS questions
Does it work / can we do it?
Are the Li+ beam currents large enough?
Are the spectra linear in backscattered energy? How good is the resolution?
Can we accumulate enough counts in a reasonable time for practical experiments?

## Slide 5
Previous work: J.A. Leavitt et al, Nucl. Instrum. & Meth. B35 (1988) 333-338

## Slide 6
Previous work: J.A. Leavitt et al, Nucl. Instrum. & Meth. B35 (1988) 333-338

## Slide 7: RBS spectrum of 3,6 MeV 7Li+ ions scattered from thin Au, Ni, Al and O films on carbon

## Slide 9: RBS spectrum of 3,0 MeV protons scattered from thin Au, Ni, Al and O films on carbon

## Slide 13: RBS formulae
Kinematic factor

## Slide 14: Ni in Si – 1,9x1016 ions/cm2 (Li+~80pA, 40 mins)

## Slide 15: P in glassy C – 6x1016 ions/cm2 (Li+~80pA, 40 mins)

## Slide 16: Zinc sheet (same conditions)

## Slide 17: Silver sheet (same conditions)

## Slide 18: Implanter calibration curves