Thermoluminescence from Semiconductor Quantum Dots

N. G. Debelo1,2, F. B. Dejene1, V. N.Mal’nev2, Teshome Senbeta2, Belayneh Mesfin2, Kitessa Roro3

1Private Bag X13, Department of Physics, University of the Free State, Qwa Qwa Campus, South Africa

2Department of Physics, Addis Ababa University, P.O.Box 1176, Addis Ababa, Ethiopia

3R and D Core (Energy Initiatives), Council for Scientific and Industrial Research, P.O.Box 395, Pretoria, South Africa

E-mail: nafsif@gmail.com

Abstract. The TL from different materials has been studied by many research groups. The simplest possible model that has been used to describe the process by which materials emit the light when heated consists of two localized levels: an isolated electron trap and a recombination center. This approach is commonly called one-trap-one-recombination center (OTOR) model. The interactive-multi-trap-system (IMTS) model has also been used. It assumes that there are one active electron trap, one thermally disconnected deep trap that cannot be thermally activated, and one recombination center. Basically, in experiment we often have more than one active electron traps taking part in TL process. In this paper, the second order kinetics describing the thermoluminescence from semiconductor quantum dots consisting two active electron trap levels and one recombination center model is proposed. The two trap levels are located at different trap depths beneath the conduction band. The rate equations corresponding to each trap level allow us to numerically simulate the variation of the concentration of electrons in both traps and the thermoluminescence intensity as a function of temperature for the semiconductor quantum dots of diameter 2-8nm. It is shown that the intensity increases with decreasing in the dot size indicating that the quantum confinement effect enhances the band to band radiative recombination rate. The two peaks of the intensity correspond to the two different active electron trap levels. With an increase in the dot size, the peaks of intensity from the deeper trap shift to the high temperature region.

Introduction

Thermoluminescence (TL) is the emission of light from materials under heating provided that they have previously absorbed the energy of irradiation [1-4]. There are three conditions necessary for the production of TL. Firstly, the material must be a semiconductor. Secondly, the material must store some energy during irradiation. Thirdly, the TL emission is triggered by heating the material. The fundamental principles that govern the TL are basically the same as those ones that govern all luminescence processes, and in this way the TL is one of a large family of luminescence phenomena [1, 2].

The light emission from semiconductor quantum dots, such as silicon, is currently active research area because of its potential applications in the silicon-based optoelectronic devices [5-8]. The efficiency of the semiconductor light emitting devices can be increased with the help of different mechanisms. In particular, the possible increasing in the intensity of TL from semiconductor quantum dots caused by the confinement have been studied in [9,11]. It was shown that the confinement increases the probability of the band to band radiative recombination and enhances the intensity of the TL.

The TL from different materials has been studied by many research groups. The simplest possible model that has been used to describe the process by which materials emit the light when heated consists of two localized levels: an isolated electron trap and a recombination center. This approach is commonly called one-trap-one-recombination center (OTOR) model [2]. The interactive-multi-trap-system (IMTS) model has also been used [12]. It assumes that there are one active electron trap, one thermally disconnected deep trap that cannot be thermally activated, and one recombination center. Basically, in experiment we often have more than one active electron traps taking part in TL process.

In this paper, we consider the model of TL with three localized levels containing two isolated active electron traps and one recombination center. It can be called two-traps-one-recombination center (TTOR) model. We consider the semiconductor quantum dots of different size with size dependent radiative recombination rate and study the variation of concentration of electrons on the traps and the intensity of the TL.

Statement of the Problem

Consider the following energy band scheme having three localized levels (figure 1). The two levels act as traps ( and ) and the other acts as recombination center (). The absorption of radiation of energy greater than the band gap energy results in the ionization of valence electrons, producing free electrons in the conduction band and free holes in the valence band respectively (transition 1). The

Figure 1:  Three level model for thermoluminescence. Allowed

transitions: (1) ionization; (2), (4) and (7) trapping; (3) and (5)

thermal release; (6) radiative recombination and emission of light.

electrons and holes may either recombine with each other or become trapped at the trap centers. In order for recombination to occur holes first become trapped at centers (R) (transition 7). Recombination takes place via the annihilation of the trapped holes by free electrons (transition 6). If the recombination transition is assumed to be radiative, then luminescence will result. The free electrons may also become trapped at levels  and  (transitions 2 and 4) in which case recombination can only take place if the trapped electrons absorb enough energy  and  respectively to be released back to conduction band (transitions 3 and 5), from where recombination is possible. In other words, the TL occurs when the trapped electrons absorb enough energy in the form of heat to be released back to the conduction band from where there is possible recombination of electrons and holes. The energy required for the trapped electrons to be released back to the conduction band is called the trap depth (activation energy). Next we write down the equations of the second order kinetics.

Let us consider two active electron traps with energy levels  and  below the bottom of the conduction band. The rate equations can be written as:

Here  is the concentration of trapped electrons on the levels  is the total concentration of traps on the levels ,  is the Boltzmann constant;  and  are the probability of electron to escape from the th trap and the re-trapping probability on the th energy level;  and  respectively are the concentration of the electrons in the conduction band and holes in the hole trap, and  is the electron-hole radiative recombination probability. It is assumed that, initially, all holes are trapped to the hole trap. The system (1-3) is closed by the quasi-neutrality condition

Basically the temperature of the system depends on time . This dependence is controlled by the conditions of experiment. The generally acceptable is the linear heating rate

where  is the heating rate. The system of equations (1-5) presents the rate equations governing the process of TL. The intensity of the TL is given by

The above presented system of equations is nonlinear with varying coefficients. It cannot be solved analytically in general case.

Results and Discussion

We solved the system of equations (1-4) numerically with the help of Mathematica 8 with the parameters  ,     1

For the typical quantum dots the retrapping probability is of the order of . We chose   and ignore the possible corrections associated with the confinement. The coefficient depends on the size of quantum dot. The graph of experimental data on the size dependence of  of semiconductor quantum dots of the radius 1−4nm is given in [5] and we summarized them in Table 1. It illustrates the rate of the radiative recombination as a function of quantum dot size for our model. Figures 2 and 3 show the variation of the concentration of electrons in the traps with activation energies  and, respectively, for quantum dots of different radii  from 1−4nm for second order kinetics model. The electrons that are released from the first trap level () can be retrapped by the deeper trap ( ). It explains an increase in the concentration of electrons in the deeper trap with temperature as indicated in figure 3. One can see from figures 2-3 that  and  depend on the size of quantum dot as well.

Table 1: Approximate values of radiative recombination rate

of the semiconductor quantum dots.

Figure 2: Numerical simulation of variation of concentration

of electrons  in the shallower trap  for the

second order kinetics.

Figure 3: Numerical simulation of variation of concentration of

electrons  in the deeper trap (  ) for the second

order kinetics.

Table 1 shows that the number of the carriers, which are recombined radiatively per unit time, increases with a decrease in the quantum dot size. Using the data of table 1 and equation (6), we simulated the temperature dependent TL intensity for the dot whose radius varies from 1nm to 4nm as presented in figure 4. The intensity increases with decreasing in the dot size indicating that the quantum confinement effect enhances band to band radiative recombination rate. There are two peaks of the TL intensity and they correspond to the two different active electron trap levels. We also found that positions of the TL intensity peaks corresponding to the first trap practically do not shift with the temperature. At the same time, the intensity peaks of the second trap shift to the high temperatures with increasing in the dot size. It is interesting that the positions of the TL maxima corresponding to the first trap practically do not change with the temperature. The maxima of TL intensity corresponding to the second trap shift to the higher temperatures with increasing the size of quantum dot. The TL peaks of the first trap are lower comparing with the ones of the second one (figure 4). It can be explained by the fact that during the excitation of the first trap only some parts of its electrons recombine with the holes emitting light. Another part of them are trapped by the second trap. This is indicated in the initial rise in the concentration of the trapped electrons in the second trap (figure 3).

Figure 4: Numerical simulation of TL intensity I versus

temperature for the second order kinetics.

Conclusion

The TL glow curves of the semiconductor quantum dots of diameter  in the model of two active electron traps and one recombination center have been numerically simulated within the frame of the first and second order kinetics approach. There are two peaks of the TL intensity corresponding to the two active electron trap levels.  Our numerical results show that the TL intensity increases with decreasing in the quantum dot size. This can be explained in terms of the quantum confinement effect [9-10]. In this paper, we account it with the help of extrapolation of the experimental data on the probability of radiative transitions on the quantum dot size [6]. We obtained that the trap with deeper electron level  (we call it the second trap) provides the higher TL intensity as compared with the trap of shallower level  (the first trap) but at higher temperatures. Both traps show increasing in the TL intensities with decreasing in the quantum dots size. We claim that this conclusion will be true for any traps provided that. The proposed model of TL in the case of quantum dots with the active electron energies  and different sizes can give a considerable increment in the second peak of TL due to the different electron-hole radiative recombination probability . The point is that  and the majority of the electrons released by the first trap will be retrapped by the second one with subsequent radiative recombination with holes. To our mind the ensemble of quantum dots of two kinds with different energy of the trapped electrons and different size of may have interesting TL properties and deserves further study.

References

[1]   S.W.S. Mckeever, Thermoluminescence of solids, Cambridge Solid State Science Series,

Oklahoma State University, 1988, pp 1-50.

[2]   Vasilis Pagonis, George Kitis and Claudio Furetta, Numerical and Practical Exercises in

Thermoluminecsnce, 2005, pp 80-100.

[3]   Yu. A. Skryshevskii, and V. A. Skryshevskii, J. Appl. Phys. 2001, pp 2711-2714.

[4]   Claudo Furetta, Handbook of Thermoluminescence, Cambridge University Press, 1988, pp 1-50.

[5]   Nidhal Mousa, Abdul-Ameer, Moafak Cadim Abdulrida, Journal of Modern Physics, 2011, 2,

pp 1530-1537.

[6]   K Dohnalova,T Gregorkiewicz and K Kusova,J. Phys.: Condens. Matter . 2014, 26, pp 1-29.

[7]   Sandro Martini, Lara Khl Teles, Marcelo Marques, Angelo E. B. Marques, Alain A. Quivy,

World Journal of Condensed Matter Physics, 2011, 1, pp 161-166.

[8]   Eun-Chel Cho, Martin A. Green, Gavin Conibeer, Dengyuan Song, Young-Hyun Cho, Giuseppe

Scardera, Shujuan Huang, Sangwook Park, X. J. Hao, Yidan Huang, and Lap Van Dao,

Advances in OptoElectronics, Hindawi Publishing Corporation, 2007, pp 1-11.

[9]   Nebiyu Gemechu Debelo and S.K. Ghoshal, Thermoluminescence from silicon quantum dots: A

Model study, Lat. Am. J. Phys. Educ., 5, No. 2, June 2011, pp 428-431.

[10]   Nebiyu Gemechu Debelo, A Model Calculation of Temperature and Size Dependent

Thermoluminescence Intensity from Silicon Nanostructures, Indonesian Journal of Physics,

22, No. 4, October 2011, pp 125-127.

[11]   Nebiyu Gemechu Debelo, The role of trap depth and trap centers in thermoluminescence from

semiconductor nanostructures, Lat. Am. J. Phys. Educ., 6, No. 2, June 2012, pp 327-329.

[12]   Vasilis Pagonis and George Kitis, Prevalence of first-order kinetics in thermoluminescence

materials: An explanation based on multiple competition processes, Phys. Status Solidi B,

March 2012, pp 1-12.