## Slide 1: Light Sources for Materials and the AfLS context
S.J.L. Billinge
CMPMS, Brookhaven National Laboratory
Department of Applied Physics and Applied Mathematics
Columbia University,

## Slide 2
"International educational exchange is the most significant current project designed to continue the process of humanizing mankind to the point, we would hope, that men can learn to live in peace--eventually even to cooperate in constructive activities rather than compete in a mindless contest of mutual destruction....We must try to expand the boundaries of human wisdom, empathy and perception, and there is no way of doing that except through education.“
[Senator J. William Fulbright, from remarks on the occasion of the thirtieth anniversary of the Fulbright Program, 1976]

## Slide 3: A synchrotron light source for Africa
Why is it important?
How would it be used?
What would it deliver?
What would it be used for?
Who would use it?
How can we get there?

## Slide 4: Why is it important?
Macro and micro challenges facing mankind:
  Energy security
  Food security
  Water security
  Environmental security
  Economic security
  Political and judicial security
  Basic freedoms to pursue happiness
Some have technological solutions, all require education, cooperation and the victory of rationality over irrationality
A facility like a synchrotron promotes cooperation, education, technology, and science
The impacts of a synchrotron go way beyond the x-rays it produces

## Slide 5: Why do I say that?
How is a synchrotron used?:
  It is a large-scale centralized scientific facility. It requires international cooperation to build and run it
  But it is used by individual scientists bringing small-scale samples from their labs.
    The synchrotron supports thousands of users in any given year
    Typical experiments last a few days and take place 1-2 times per year
It is a focal point for a scientific community
  A diaspora of scientific users meet each other and overlap at the synchrotron when they do experiments, forming a geographically diverse community
It is inclusive, not exclusive
  Materials scientists, earth scientists, biologists, chemists, physicists, conservation scientists, paleontologists, pharmaceutical scientists, polymer scientists, and so on and so forth
All Materials are made of atoms, synchrotrons allow us to study atoms

## Slide 6: What would it deliver?
Science (we have heard about this already this week)
Technology (we have heard about this too)
A focal point for a LARGE and diverse community of scientists across Africa
  Education for that community
  Inspiration & a sense of pride for that community
  World class facilities for that community
  A high profile international stage for the science coming from that community
The synchrotron will be built in one place, but it will be used by people from across Africa to solve problems all across Africa

## Slide 7: What would it deliver?
Computer science => The Internet of Things (IoT)
Synchrotron Science => The science of things (SoT)

## Slide 8: Nanoscience
How can we characterize material structure when they are nano-structured?

## Slide 9: The atomic Pair Distribution Function
Raw data
Structure function
PDF

## Slide 10: What is the PDF?
Sit on an atom and look at your neighborhood
G(r) gives the probability of finding a neighbor at a distance r
PDF is experimentally accessible
PDF gives the local structure

## Slide 11: The Atomic Pair Distribution Function (PDF) Method
Use modern high intensity x-ray and neutron sources to collect unprecedentedly precise data
Utilize all the information: Bragg and diffuse scattering
Use modern computing capabilities to analyze, model and visualize the data
Chupas et al., J. Appl. Crystallogr. (2003)
Billinge-group, BNL, SUNY-SB, APS collaboration
Main developments thanks to Pete Chupas and Xiangyun Qiu

## Slide 12: Nanostructure refinement
5.11Å
4.92Å
4.26Å
3.76Å
2.84Å
2.46Å
1.42Å
Pair distribution function (PDF) gives the probability of finding an atom at a distance “r” from a given atom.
5

## Slide 13: Quantum Dot solar cells

## Slide 14: CdSe quantum dots
RAPDF experiments at APS, Sector 6
Work of grad student Ahmad Masadeh
Masadeh, SJB et al. PRB 76, 115413 (2007)

## Slide 15: Structure of the CdSe core
Wurtzite structure
Zinc blende structure

## Slide 16
Masadeh, SJB et al. PRB 76, 115413 (2007)
Thanks to Reinhard Neder for help with stacking fault models

## Slide 17: Size of the structural core
Masadeh, SJB et al. PRB 76, 115413 (2007)
Also see Shamoto paper, JAC 2007

## Slide 18: White Light Nanoparticles
Samples are from Sandy Rosenthal (Vanderbilt)

## Slide 19: Thermoelectric materials
Evolution of Ir dimers vs T in Li2RhO4
Knox, Bozin, sjlb et al, PRB 13
Evolution of anharmonicity/off centering in SnTe
Knox, Bozin, SJLB et al PRB 14

## Slide 20: Materials for chemical separations

## Slide 21: High throughput allows studies of in-situ synthesis
We can see precursor species in solution
We can measure Nanoparticle structural parameters
High energy x-rays can penetrate relatively thick walled vessels
=> Let’s do in-situ studies of synthesis
Rich collaboration with the group of Bo Iversen (Aarhus)
Image credit Christoffer Tyrsted

## Slide 22: PDF analysis of in situ SnO2 formation
in-situ studies of SnO2 formation during hydrothermal synthesis,
PDF measured every 7 seconds at an synchrotron x-ray source
measured PDFs were fitted as a two-phase mixture of SnCl4.2H2O molecules and SnO2 crystallites
time dependence of the precursor-target ratios and the crystallite size
K. M. Jensen, et al., J. Am. Chem. Soc., 134, 6785 (2012)
SnCl4O2
SnO2

## Slide 23: In-situ study of hydrothermal synthesis of yttria-stabilized zirconia nanoparticles
Christoffer Tyrsted1, Nina Lock1,2, Kirsten M. Ø. Jensen1, Mogens Christensen1, Espen D. Bøjesen1, Hermann Emerich3, Gavin Vaughan4, Simon J. L. Billinge5,6*, Bo B. Iversen, under review
Precursor

## Slide 24: In-situ study of hydrothermal synthesis of yttria-stabilized zirconia nanoparticles
Christoffer Tyrsted1, Nina Lock1,2, Kirsten M. Ø. Jensen1, Mogens Christensen1, Espen D. Bøjesen1, Hermann Emerich3, Gavin Vaughan4, Simon J. L. Billinge5,6*, Bo B. Iversen, under review
Amorphous
intermdiate

## Slide 25: In-situ study of hydrothermal synthesis of yttria-stabilized zirconia nanoparticles
Christoffer Tyrsted1, Nina Lock1,2, Kirsten M. Ø. Jensen1, Mogens Christensen1, Espen D. Bøjesen1, Hermann Emerich3, Gavin Vaughan4, Simon J. L. Billinge5,6*, Bo B. Iversen, under review
Nanocrystalline
final product

## Slide 26: ctDPF of Catalysts
Experiments on ID15 at ESRF
Pt/PtO nanoparticle catalyst on a g-alumina support in a flow rig
Have a fully refinable PDF in every pixel of the image
Large particle size in a shell around the rim, small particle size and much lower density in the middle
=> Spatially resolved, time resolved nanostructure studies
S. D. M. Jacques, Di Michiel, SJLB et al. Nat. Commun. 4, 2536 (2013)

## Slide 27: ctPDF of Battery materials
10,000 2D datasets per image, 30 mins per image
~10Tb/day
Jensen, Corr, Di Michiel, SJLB et al., J. Electrochem. Soc. (2015)

## Slide 28: Characterizing nanoparticles of APIs in suspension
Samples were API particles of various sizes and in various concentrations in aqueous suspension
These are drugs for nebulizer applications
The goal was to characterize the structure and nanoparticle size in the different suspensions.

## Slide 29: Characterizing nanoparticles of APIs in suspension
Green: PDF of the crystalline control sample
Blue: PDF of the aqueous solvent
Reproducibility!
High-r region from the crystalline control and sediment from a high concentration suspension

## Slide 30: Thin film PDF at normal incidence
Jensen, Iversen, Johnson, Dooryhee SJLB et al. IUCrJ 2015

## Slide 31: Recrystallization from the amorphous state: Lactose
Lactose is a common excipient for pharmaceutical tableting
Commercially available in crystalline or amorphous forms
A-form can be prepared from α-Monohydrate crystals by spray-drying, melt quenching, and lyophilization
Collaboration with Eugene Cheung,
Paul Krolikowski, and Steve Hollis (Amgen Inc.)

## Slide 32: Time dependent studies
Various A-form samples aged at, 40°C/75% RH

## Slide 33: Time dependent studies
How does the crystallinity grow in?

## Slide 34: The science of things
Computer science => Internet of Things (IoT)
Synchrotron science => Science of Things (SoT)

## Slide 35: How do we get there?
Work on the politics/economics (top down)
Build the community (bottom up)
Educate the community
Build the community

## Slide 36: Building and educating the Materials Science Research community in Africa

## Slide 40
Students working in groups

## Slide 41: Group research proposal activity
Using dyes from local plants as photoactive material in dye-sensitized solar cells
Making activated carbon for supercapacitor applications from waste streams of coffee production (were in Addis Ababa)
Developing an online research portal for the JUAMI community: the JUAMI research exchange
A collaboration to share hands-on learning materials and learning modules between US and African Universities

## Slide 45
Juami facebook page
Juami Research Exchange

## Slide 46
Arusha, Tanzania; May 29 – June 10, 2016
Theme: Materials for Sustainable Energy
Local Host Institution: Nelson Mandela African Inst. Sci. & Tech.
Joint Undertaking for an African Materials Institute
Morning tutorials
Afternoon learning activities
Evening research lectures
~ 20 instructors
~ 60 students: 25 US + 35 African
By application, participation fully funded
http://www.columbia.edu/cu/juami/
US Organizing committee:
Simon Billinge, Peter Green, Sossina Haile
Columbia Univ., Univ. of Mich., Northwestern
Intense learning in a multi-cultural environment
At the base of Mt. Kilimanjaro
To receive announcements: join the JUAMI group on facebook

## Slide 47: Bottom up: ways to get started?
Educate and advertise capabilities.
  Workshops (like this one!)
  Schools (like JUAMI but with a heavy synchrotron component)
  MOOCs
Clearing house of mentors.
  Engage young researchers (e.g., JUAMI fellows)
  Online community of synchrotron researchers
  Collaborate to make beamtime requests
  Collaborate on data analysis
Program of embedding African scientists in experienced Mentor groups (needs funding)
Mail in access to existing synchrotrons
Collaborative beamtimes
Autonomous beamtimes
Involvement in building and running beamlines (partner User agreements)

## Slide 48
Massively Open Online Courses and the African Lightsource
MOOCs are changing everything about education
Access, distribution, metrics and learning science
A collaboration with Lawrence Norris

## Slide 49: Training Opportunities for African Lightsource and synchrotron users everywhere
Using a MOOC platform (like OpenEdX) it is possible to have a web portal branded as an africanlightsource.org site that taps into an entire worldwide library of courses and training modules.
Online training institute hosted on OpenEdX
http://training.africanlightsource.org
Couple this with an online community of practice on wordpress/Google groups etc.
http://community.africanlightsource.org

## Slide 50: Summary
African Light Source will happen. The questions are more when? And how? Than whether?
Top down activities by high level people
Bottom up activities by African scientists (with a bit of help from their friends around the world)

## Slide 51
#1 Open edX Provider for Higher Ed
Platform Deployment & Course Design

## Slide 52
1 - Innovation with full autonomy 2 - Ability to launch an unlimited number of branded instances 3 - Full control of analytics - no shared data 4 - Pedagogical research.
Discover new interactive activities 5 - No licensing or royalty fees
6 - No revenue sharing with third-party orgs 7 - New entrepreneurial, e-commerce initiatives 8 - Implementation of new content marketing strategies 9 - Prospect generation and new enrollments
10 - A new path towards alumni engagement
11 - New learning features and integrations
WHY